Supplementary data file

N

H

N

N

O

C

l

O

O

O

O

O

O

H

O

O

H

O

H

O

H

O

H

H

O

O

H

O

H

(

Bb

)

(

A

)

Figure 1:  Structure of AMX (A) and NG (B)

Figure 2: DSC analysis of pure AMX (A), pure NG (B), lipids (C), physical mixture (D), AMX-NG SLNs (E), AMX-SLNs (F), NG-SLNs (G), blank-SLNs (H)

Figure 3:  FT-IR spectra of pure AMX (A), pure NG (B), AMX-SLNs (C), NG-SLNs (D), and blank SLNs (E)

Figure 4: AMX particle size distribution

Figure 5: AMX zeta potential

Figure 6: NG particle size distribution

Figure 7: NG zeta potential

Table 1. Summary of the micromeritics parameters like (PS, ZP, PDI) and EE & DL.

|  | Micromeritics (PS, ZP, PDI) and EE & DL |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Drugs | Trials | Particle size (nm) | PDI | Zeta potential (mV) | Entrapment efficiency (%) | Drug loading (%) |
| AMX-SLNs | 1 | 110.1 | 0.366 | -27.6 | 62.1 | 4.14 |
|  | 2 | 65.93 | 0.259 | -22.9 | 61.6 | 4.07 |
|  | 3 | 70.82 | 0.296 | -25.3 | 59.8 | 3.9 |
|  | Average | 82.28 | 0.307 | -25.26 | 61.16 | 4.07 |
| NG SLNs | 1 | 113.4 | 0.458 | -18.1 | 79.1612 | 9.8 |
|  | 2 | 80.69 | 0.305 | -27.4 | 79.17753 | 9.89 |
|  | 3 | 84.03 | 0.285 | -31.5 | 79.13404 | 9.89 |
|  | Average | 92.70 | 0.349 | -25.66 | 79.15761 | 9.8 |

Table 2. Colloidal stability studies of AMX-SLNs and NG-SLNs:

| Drugs | Time (hours) | Batch no. | Particle size (nm) |  | PDI |  | Zeta potential (mV) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Room temp. | 4 °C | Room temp. | 4 °C | Room temp. | 4 °C |
| AMX-SLNs | 6 hours | Batch 1 | 65.93 | 94.92 | 0.257 | 0.373 | -22.9 | -23.6 |
|  |  | Batch 2 | 48.97 | 47.62 | 0.364 | 0.352 | -22.3 | -21.1 |
|  |  | Batch 3 | 61.26 | 61.69 | 0.398 | 0.453 | -17.22 | -18.8 |
|  | 12 hours | Batch 1 | 64.46 | 94.12 | 0.203 | 0.389 | -20.8 | -19.4 |
|  |  | Batch 2 | 69.6 | 66.68 | 0.333 | 0.378 | -8.76 | -17.85 |
|  |  | Batch 3 | 41.96 | 61.32 | 0.264 | 0.407 | -21.6 | -22.4 |
|  | 24 hours | Batch 1 | 64.65 | 70.82 | 0.201 | 0.296 | -13.2 | -25.3 |
|  |  | Batch 2 | 103.6 | 88.85 | 0.298 | 0.221 | -5.47 | -15.7 |
|  |  | Batch 3 | 53.14 | 64.75 | 0.346 | 0.465 | -12.9 | -27 |
|  | 48 hours | Batch 1 | 87.7 | 69.24 | 0.277 | 0.269 | -10.8 | -16.27 |
|  |  | Batch 2 | 76.92 | 65.14 | 0.300 | 0.365 | -19.5 | -12.6 |
|  |  | Batch 3 | 65.57 | 77.77 | 0.372 | 0.378 | -8.76 | -14.3 |
| NG SLNs | 6 hours | Batch 1 | 84.03 | 85.04 | 0.285 | 0.315 | -31.5 | -31.4 |
|  |  | Batch 2 | 81.9 | 81.66 | 0.327 | 0.328 | -31.1 | -29.9 |
|  |  | Batch 3 | 78.99 | 78.34 | 0.266 | 0.281 | -29.8 | -30.1 |
|  | 12 hours | Batch 1 | 83.4 | 82.19 | 0.274 | 0.283 | -33.2 | -32.4 |
|  |  | Batch 2 | 80.87 | 81.46 | 0.303 | 0.314 | -30.2 | -30.2 |
|  |  | Batch 3 | 77.05 | 77.05 | 0.278 | 0.277 | -28.2 | -28.2 |
|  | 24 hours | Batch 1 | 82.79 | 84.81 | 0.322 | 0.302 | -16.4 | -9.43 |
|  |  | Batch 2 | 77.36 | 80.82 | 0.312 | 0.359 | -13.1 | -9.63 |
|  |  | Batch 3 | 79.34 | 76.95 | 0.276 | 0.314 | -10.2 | -13.3 |
|  | 48 hours | Batch 1 | 82.09 | 95.2 | 0.284 | 0.422 | -7.94 | -8.70 |
|  |  | Batch 2 | 79.13 | 87.22 | 0.281 | 0.405 | -8.32 | -6.4 |
|  |  | Batch 3 | 77.46 | 79.22 | 0.255 | 0.316 | -6.47 | -11.7 |

## Table 3. Kinetic modelling on drug release from pure and controlled drug delivery system (AMX-SLNs and NG-SLNs)

| Formulation type | Parameters |  | Release kinetic modelling type |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Zero order | First order | Higuchi model | Korsmeyer-Peppas model | Hixson Crowell model |
| AMX-SLNs | Slope | 2.595 | 0.0918 | 0.4088 | 0.0399 | 0.0925 |
|  | Intercept | 18.443 | 2.944 | 0.1172 | 0.3385 | 2.6631 |
|  | Regression coefficient (R2) | 0.8655 | 0.7723 | 0.9485 | 0.7723 | 0.8062 |
| NG-SLNs | Slope | 5.5544 | 0.3258 | 0.4088 | 0.1415 | 0.2619 |
|  | Intercept | 2.0739 | 1.1916 | 0.1172 | 1.1416 | 1.4136 |
|  | Regression coefficient (R2) | 0.9315 | 0.7771 | 0.9485 | 0.7771 | 0.8485 |

Table 4. Estimated Average Binding Affinities of the top poses of the chosen compounds for CYP3A4 and CYP2D6

| Drugs | Binding affinity (kcal/mol) |  |
| --- | --- | --- |
|  | CYP3A4 | CYP2D6 |
|  | 5TE8 | 4WNU |
| AMX (PubChem CID-2170) (CHEMBL1113) | -9.162 | -8.373 |
| NG (PubChem CID 442428) (CHEMBL451532) | -9.551 | -10.49 |