Article title: QbD-based development of ultradeformable nanovesicular transgelosome of standardized Piper longum extract for melanoma

Short running title: Nanovesicular transgelosome for melanoma therapy

Author names: Debadatta Mohapatra1, Dulla Naveen Kumar2, Singh Shreya1, Dhananjay Panigrahi3, Ashish Kumar Agrawal2, and Alakh N Sahu1*

Author affiliations:

1Phytomedicine Research Laboratory, Department of Pharmaceutical Engineering & Technology, IIT (BHU), Varanasi-221005, Uttar Pradesh, India

2Nanomedicine Research Laboratory, Department of Pharmaceutical Engineering & Technology, IIT (BHU), Varanasi-221005, Uttar Pradesh, India

3Dr. Reddy's Laboratories, Hyderabad, Telangana, India

ORCID iD:

Debadatta Mohapatra: 0000-0003-3044-8706

Dulla Naveen Kumar: 0000-0003-2415-7806

Singh Shreya: 0000-0002-9242-9597

Dhananjay Panigrahi: 0000-0002-3205-9897

Ashish Kumar Agrawal: 0000-0002-7302-3647

Alakh N Sahu: 0000-0002-2378-6179

*Author for correspondence:

Alakh N Sahu

E-Mail: ansahu.phe@iitbhu.ac.in

Tel.: +91 9451137862

# Methodology

## High-performance liquid chromatography (HPLC)

HPLC study was carried out using an Agilent HPLC system (Agilent 1260 Infinity II) furnished with a quaternary pump (1260 Quat Pump VL)), autosampler (1260 Vial Sampler), column (QuasarTM C18 LC column, PerkinElmer, 250 × 4.6 mm with 5 μm particle size), a standard flow cell (13 μL, 10 mm, and 120 bar), diode array detector (1260 DAD WR), and Open LAB CDS EZChrom Workstation VL software. With 80:20 v/v ratio of HPLC grade methanol and water as the mobile phase, the isocratic elution was carried out at a flow rate of 1.00 mL/min for 10 min. The developed HPLC method was as per the International Conference on Harmonization Tripartite Guideline (ICH Topic Q 2 (R1), Step 4 version, Validation Of Analytical Procedures: Text And Methodology ) [1].

### Preparation of primary stock solution and working standard solution

The individual primary stock solutions of PIP and PLGN (1 mg/mL) and the working standards (2-30 μg/mL) were prepared by diluting suitably with HPLC-grade methanol. Before the HPLC analysis, the standard solutions were vortexed, bath sonicated for 5 min, filtered through a 0.22 μm syringe filter, stored in the amber-colored volumetric flask, and kept at 4°C. Twenty microliters of samples were injected into the HPLC using an autosampler.

### Validation of the HPLC method

The analysis was carried out in triplicate, and the calibration curves were made by graphing the average area (mAU) v/s the corresponding concentration (μg/mL). The HPLC method was validated for linearity, range, accuracy (% recovery), precision (intermediate precision and repeatability), limit of detection (LOD), limit of quantification (LOQ), robustness, and system suitability test as per ICH Topic Q 2 (R1) [1].

#### Linearity and range

The linearity and range of the method were verified from the correlation coefficients obtained from the calibration curves of PIP and PLGN.

#### Accuracy

From the percentage recovery by the standard addition method at three levels (50, 100, and 150%), the accuracy of the HPLC method was examined. Accurately different concentrations (4, 8, and 12 μg/mL) of working standard solution were added to a pre-analyzed sample (8 μg/mL) and analyzed by the HPLC method.

The percent recovery was estimated by Equation S1.

% recovery=Experimental concentration Theoritical concentration×100                          (Eq.  S1)

#### Precision

To establish the precision of the devised HPLC method, studies on repeatability and intermediate precision were conducted. Six replicates of each working standard were analyzed by the HPLC, and the repeatability was evaluated from the percent relative standard deviation (% RSD) of the obtained area.   By examining the chromatographic area of three concentrations (6, 12, and 18 µg/mL) and determining the % RSD, the intermediate precisions (intra-day and inter-day) were evaluated.

#### Limit of Detection (LOD) and Limit of Quantification (LOQ)

The LOD and LOQ were estimated using Equation S2 and Equation S3, respectively.

LOD=3.3 SDS                                     (Eq.  S2)

LOQ=10 SDS                                     (Eq.  S3)

Where the SD is the average standard deviation of responses (y-intercept), and S is the average slope of calibration curves

#### Robustness

Intentional modifications in various chromatographic settings were used to test the robustness of the devised HPLC technique. Modifications in wavelength, run times, flow rate, and mobile phase composition were made and analyzed for changes in the peak area of PIP and PLGN, each of 12 μg/mL.

#### System Suitability

System suitability constraints were used to examine the consistency of the HPLC performance. Six replicates of each working standard (12 μg/mL) were injected, and parameters like % RSD retention time (Rt), % RSD of peak area, capacity factor, number of theoretical plates, peak purity, and tailing factor were evaluated.

## Authentication of Piper longum fruits, extraction, and standardization

The collected fruits of Piper longum (P. longum) were authenticated by Prof. N.K Dubey, Department of Botany, Institute of Science, Banaras Hindu University, and the voucher specimen (Pipera.2021/6) was submitted to the herbarium of the Department. The fruits were coarsely powdered and extracted via microwave irradiation (450 W, 5 min, domestic micro wave oven, HOTBLASTTM, Samsung, South Korea) followed by triple maceration using absolute ethanol at a ratio of powder to solvent 1:4 w/v. The obtained ethanolic extract was filtered (Cellulose nitrate membrane filters, 0.45 μm, 47 mm diameter), concentrated by rotary vacuum evaporator (IKA®, RV 10, Germany) at 40°C with 60 rpm, and kept in a refrigerator until usage. The P. longum fruits ethanolic extract (PLFEE) was standardized for PIP and PLGN by a validated HPLC method. Briefly, a known amount of PLFEE was mixed with ethanol, vortexed, bath sonicated (10 min), and filtered through a 0.2 μm syringe filter. The filtrate was suitably diluted with HPLC grade methanol, and 20 μL of the sample was injected into the HPLC system for the quantification of PIP and PLGN by validated HPLC method at their respective absorption maxima (λmax of PIP: 342 nm and PLGN: 340 nm).

## Formulation and Development of transferosome (TFs) of standardized PLFEE

Standardized PLFEE-loaded TFs formulations were prepared by the thin-film hydration-based rotary evaporation method. The required amount of Phospholipon® 90 H (PL-90 H), Tween® 80 (T-80), and 250 mg of standardized PLFEE was mixed with 40 mL of absolute ethanol in a 100 mL round-bottom flask and subjected to a bath sonicator for 30 min to achieve solubilization and molecular interaction of PLFEE with excipients.  Afterward, the ethanol was evaporated with a rotary vacuum evaporator at 40° C, 70 rpm, until a thin film was formed inside the walls of the flask. The residual solvent trace from the film was removed under vacuum (for 6 h) and hydrated with Type-I ultra-pure water for 1 h by shaking with an orbital shaker (REMI, RS 12 plus) to produce transferosome (TFs) vesicles. The vesicle size reduction was achieved by probe sonication (Hielscher ultrasound technology, Germany) at 80% amplitude with 1 cycle (at an interval of 120 seconds) for a different time as per the experimental design. Briefly, the TFs were poured into a screw-capped glass vial and placed in an ice-filled beaker before probe sonication to avoid degradation due to heat during probe sonication.  The unentrapped extract was removed by centrifugation and discarding the supernatant. Then the TFs was stored and protected from light at 4° C.

## Response surface methodology (RSM) and optimization

RSM was used to examine the influence of critical material attributes (CMAs), such as the quantity of PL-90 H (X1 = mg), the quantity of edge activator or T-80 (X2 = mg), and critical process parameters (CPP), like probe sonication time (X3 = min) on critical quality attributes (CQAs), such as average hydrodynamic vesicular size (Y1 = Zavg), entrapment efficiency of major bioactive component PIP (Y2 = % EE), and flexibility of TFs (Y3 = Flexibility). The RSM was studied using a 3-factors, 5-level rotatable (α value of 1.681) central composite design (CCD) via a Trial version of Design-Expert® software (Version-12, Stat-Ease Inc., Minneapolis, MN, USA).  Preliminary experiments were conducted to identify the possible ranges of the independent variables that have a strong influence on the several dependent variables (Zavg, % EE, and flexibility) chosen for this investigation. A total of 20 batches (6 replications of central points + 6-star points (axial points) + 8 cube points (factorial points)), were produced by the software. The experimental results (CQAs) of 20 batches were fed into the software, and analyzed by analysis of variance (ANOVA) to investigate model adequacy and significance (p<0.005).  Statistical parameters, such as correlation coefficient (R2), model F-value, model p-value, lack of fit F-value, lack of fit p-value, the difference between predicted and adjusted R2 value, and adequate precision (signal to noise ratio) were considered to investigate model adequacy. To envisage the best TFs formulation, the model was fitted to linear, two-factor (2F) interactions, quadratic, and cubic models. The software-generated polynomial equations were used to examine factor–response relationship. The interaction effect of the CMAs and CPP on the CQAs was also observed using response surface graphs. Optimum CMAs and CPP essential for the development of desired TFs (high % EE, acceptable particle size, and optimum flexibility) were acquired by numerical and graphical optimization techniques available in the software. Finally, the predictability of the rotatable CCD model was verified by formulating checkpoint batches (n = 5) of optimized TFs formula as suggested by Design-Expert software and evaluating the corresponding CQAs. A quantitative comparison was made between the experimental values and software-based theoretical prediction by calculating the percentage prediction error by Equation S4.

% prediction error=Experimental result-predicted resultPredicted result×100                (Eq.  S4)

## Characterization of TFs

### Organoleptic characteristics and pH

The prepared TFs were evaluated for color, clarity, homogeneity, transparency, etc. The pH of TFs was measured in triplicate at 25°C using a digital pH meter (PC 700, Eutech Instrument, Singapore) which was previously calibrated using pH 4, pH 7, and pH 10 buffer solutions.

### Refractive index (RI)

The RI of all the TFs was estimated to verify the isotropy of the TFs formulations by estimating and comparing the RI of samples collected from three different regions of each TFs formulation. It was determined by a digital Abbe-type refractometer (Labman Scientific Instruments Pvt. Ltd., India) equipped with a Tungsten lamp, refractometer prisms, monocular system, temperature controller, and telescopic adjustment system at 25 ± 1°C. Briefly, the prisms were cleaned thoroughly, and a few drops of the undiluted TFs were spread evenly on the surface of the lower illuminating prism for measuring the RI. The experiment was carried out in triplicates, and the average results were reported.

### Entrapment Efficiency (EE) and Loading Capacity (LC)

EE for major active constituent (PIP) was estimated by the validated HPLC method. The ultracentrifugation method was used to separate the un-entrapped PIP (free drug) in supernatant from the encapsulated drug in pellet form. Briefly, each formulation was centrifuged at 100,000 g at 4°C for 1 h using an ultracentrifuge (Beckman Optima XPN-100, Palo Alto, CA, USA) with an SW 90 Ti rotor. The quantity of PIP in the supernatant after the centrifugation was estimated by the HPLC method at 342 nm after suitable dilution with HPLC-grade methanol. The EE was then calculated by Equation S5.

EE (%)=PIPT-PIPSPIPT×100                                            (Eq. S5)

Where EE is the entrapment efficiency, PIPT is the total amount of PIP in the formulation (amount of PIP in 100 mg of PLFEE), and PIPs is the amount of free PIP in the supernatant after centrifugation.

The LC was calculated as per Equation S6.

LC (%)=PIPT-PIPSExcT×100                                            (Eq. S6)

Where LC is the loading capacity, PIPT is the total amount of PIP in the formulation, PIPs is the amount of free PIP in the supernatant after centrifugation, and ExcT is the total amount of excipient used in the formulation.

### Hydrodynamic vesicle size (Zavg), polydispersity index (PDI), and zeta potential (ζ)

The Zavg, PDI, and ζ of TFs were measured using a dynamic light scattering instrument (Zetasizer Pro, Malvern Panalytical Ltd., UK) equipped with ZS Xplorer software (version 2.3.1) at a scattering angle of 173° at 25°C. The Zavg and PDI were acquired using a polystyrene disposable cuvette (DTS0012), whereas the ζ was measured using a universal dip cell (ZEN1002) having palladium electrodes with 2 mm spacing. Each of the TFs was diluted 20 times with Type-I ultra-pure water and filtered through a 0.45 µm polyvinylidene fluoride (PVDF) syringe filter (AXIVA Sichem Pvt. Ltd.) to avoid multiple scattering effects.

### Flexibility

The vesicular flexibility was measured via an in-house fabricated device (Figure S4) by passing the TFs through a membrane filter (0.05 µm), connected to a vacuum pump (Axiva, chemVk V300, Haryana, India). Each formulation was diluted with 10 mL of water and a pass through the membrane filter under a constant vacuum (30 mm Hg) for 5 min. The flexibility was calculated as an indicator of elasticity using Equation S7 [2].

F=Jrvrp2                                            (Eq.S7)

where F is the flexibility (mL/s), J is the amount of dispersion filtered (mL) per unit time (s), rv is the size of vesicles after extrusion (nm), rp is the pore size of the filter membrane (nm).

### Optical Microscopy

Microscopic images of optimized TFs were captured (at 4X and 10X magnification) by a digital microscope (Magnus MLX Plus, Olympus Opto Systems India Pvt. Lt d., Uttar Pradesh, India) equipped with a digital camera (5.1 MP, Magcam DC 5, ½.5” CMOS Sensor) and Magvision software (version x36, 3.7.6820). The optimized TFs were dropped on a glass slide and subjected to the microscope for analyzing vesicular structure.

### High resolution Scanning electron microscopy (HRSEM)

HRSEM photomicrographs of optimized TFs were taken using a high-resolution scanning electron microscope (FEI NovaTM Nano SEM 450, FEI, USA) equipped with Everhart–Thornley detector (ETD) and xT Microscope software control software (version 1.0) at an accelerating voltage of 15 kV. The optimized TFs were dropped onto a clean glass slide (1 cm2) and dried overnight at room temperature to obtain a thin film. Before subjecting to the instrument, the sample was mounted on an aluminum stub using double-sided carbon tape followed by sputter coating by a desk sputter coater (DSR 1, Nanostructured Coating Co., Iran) with palladium and gold at a ratio of 40:60 w/w for 2 min.

### Scanning probe microscopy (SPM)

The analysis was performed using an SPM instrument (NTEGRA Prima, NT-MDT Service, and Logistics Ltd.) equipped with Nova Px software (version 3.4.0). The sample was dropped onto a clean glass slide, dried naturally, and subjected to the instrument for morphological analysis.

### High-Resolution Transmission Electron Microscopy (HRTEM) and selected area electron diffraction (SAED) analysis

The HRTEM and SAED patterns of optimized TFs were examined to investigate the vesicular morphology and crystallinity. The analysis was carried out using a high-resolution transmission electron microscope (TECNAI G2 F20 TWIN, FEI, USA) equipped with high angle annular dark field (HAADF) detector, and Gatan’s Digital Micrograph software (version 3.7.4) at 200 kV using a carbon-coated copper grid (Ted Pella, 400 Mesh, 3.05 mm diameter). The TFs samples were diluted 20 times with Type-I ultra-pure water, filtered through a 0.45 µm syringe filter, and 20 μL of the diluted TFs was dropped onto the TEM grid and dried overnight at room temperature. The excess amount of the sample was removed by soaking it in soft tissue paper. The HRTEM photomicrographs were analyzed by ImageJ software (National Institutes of Health (NIH), Bethesda, Maryland, version 1.53e, Java 1.8.0_172), and the average size was calculated.

### Drug excipient compatibility study

The drug excipient compatibility was studied by attenuated total reflectance-Fourier transform infrared spectroscopy (ATR-FTIR) and High-performance thin layer chromatography (HPTLC).

#### Attenuated total reflectance-Fourier transform infrared spectroscopy (ATR-FTIR)

ATR-FTIR analysis of standardized PLFEE, PL-90H, physical mixture, and optimized TFs were carried out to predict the possible interaction between PLFEE and excipients using an ATR-FTIR spectrophotometer (Bruker Alpha II, Bruker Optics, Ettlingen, Germany) equipped with an attenuated total reflectance (ATR) accessory. Since the optimized TFs are liquid, it was freeze-dried for 12 h (LFD-BT-101, Labocon Scientific Limited, UK) before ATR-FTIR analysis to avoid the broad peak of water. Data acquisition was made using OPUS software (Version: 7.0) within the wavenumber of 4000 to 400 cm−1 with 4 cm-1 spectral resolution and 40 scans.

#### High-performance Thin Layer Chromatography (HPTLC)

The compatibility of PLFEE with the TFs excipients was further analyzed by HPTLC fingerprinting. The chemical integrity of PIP and PLGN in the ethanolic extract PLFEE, physical, and optimized TFs was investigated by qualitative fingerprinting analysis with HPTLC instrument (CAMAG) equipped with WinCATS software (Version: 1.4.7.2018). Fingerprinting was carried out on 20×10 cm silica gel 60 F254 precoated aluminum plates (E. Merck, Darmstadt, Germany). Pure PIP, PLGN, PLFEE, physical mixture, and optimized TFs were dissolved in ethanol and centrifuged (10000 rpm for 5 min), and the supernatant was used for HPTLC fingerprinting. Accurately 5 μL of each sample solution was applied in triplicate on a pre-coated aluminum plate (1st band x = 15 mm, y = 8 mm) at a dosage speed was 100 nL/s with 8 mm band width by Linomat V sample applicator (CAMAG, Switzerland) attached with 100 μL CAMAG syringe. Then, the plate was developed in a pre-saturated twin trough glass chamber (CAMAG, 20 x 10 cm) up to 90 mm distance using 10 ml of mobile phase (toluene: ethyl acetate (6:4 v/v)) and dried by hair drier (Philips India Ltd., India). Then the dried plate was scanned by HPTLC scanner (CAMAG TLC Scanner IV) at a scanning speed of 20 mm/s with a slit dimension of 6.00 × 0.45 mm micro at 254, 340, 342, and 366 nm wavelength. The values of the retardation factor (Rf) of pure phytoconstituents and the samples were compared to predict possible drug-excipient compatibility [3]. The fingerprint of the developed plate was visualized in CAMAG TLC Visualizer 2 and photographs were captured by the charge-coupled device (CCD) camera (SONY, Super HAD, HDR).

### Polarized Light Microscopy (PLM)

PLM images of PLFEE, PL-90H, physical mixture, and freeze-dried optimized TFs (TFs FD) were captured at 10X magnification using a polarizing microscope (Radical RXLr-5, New Delhi, India) furnished with a digital microscopic camera (Procam, 5 MP) and Radical ProCam software (Version 3.7) under the crossed polarizer analyzer arrangement at 25° C. Samples were sprinkled on a microscopic glass slide and subjected to the polarizing microscope. Samples were inspected under various setups, including plain polarized light to crossed polarized light (XPL) at various angles (from 0° to 120°) by rotating the analyzer slider fitted at the top.

### X-ray diffraction (XRD)

The crystallinity of PLFEE, PL-90H, T-80, physical mixture, and optimized TFs was examined by a desktop X-ray diffraction system (Rigaku Miniflex 600; Tokyo, Japan) using Ni-filtered Cu Kα radiation (λ = 1.5406 A°) at current 15 mA and voltage 40 kV. The XRD pattern was recorded using MiniFlex Guidance software (Version 2.0.2.1) over a range of 2 Theta from 10° to 100° with a step size of 0.02°/step at a scan speed of 7°/min at 25°C. Since Tween® 80 is viscous, the drop cast technique was used to examine its XRD pattern by preparing a thin film of the sample on a glass plate via dropping and drying at 40°C.

### Differential scanning calorimetry (DSC)

DSC of PLFEE, PL-90H, physical mixture, and the optimized TFs were carried out using a DSC apparatus (DSC 60 Plus, Shimadzu, Japan), equipped with TA-60WS Collection software (Version 2.21). An empty pan was used as the blank, and the instrument was calibrated with indium (melting point of 156.6 °C) before the examination. Approximately 5 mg of each sample was placed in a pierced aluminum pan and kept in the thermal chamber of the DSC. The analysis was carried out at a linear heating rate of 10°C/min from 25 to 350°C in a nitrogen atmosphere at a flow rate of 100 mL/min.

### Thermogravimetric analysis (TGA)

TGA analysis of PLFEE, PL-90H, physical mixture, and the optimized TFs was carried out using TGA apparatus (Shimadzu TGA-50 analyzer, Shimadzu, Japan) equipped with TA-60WS Collection software (Version 2.21). The analysis was performed under a stream of nitrogen (flow rate of 100 mL/min) by linearly heating the samples (~10 mg) from 10 to 800°C (heating rate of 10 °C/min) in a platinum pan.

### Stability study

The stability testing of optimized TFs was carried out as per ICH guidelines (ICH Q1 R2). The optimized TFs were filled in the sterile glass vial and subjected to long-term stability condition (5 ± 3°C) for 12 months and accelerated condition (25 ± 2°C/60 ± 5% RH) for 6 months. Periodically (long term: at 0, 6, 9, and 12 months; accelerated condition: 0, 3, and 6 months), the formulations were evaluated for evaluating stability. Further, the stability of the optimized TFs was also evaluated under stress conditions, such as heating-cooling and freeze-thaw cycle. The stability was accessed after 3-cycles of a heating-cooling cycle (one cycle: 40°C and 4°C each for 24 h), and freeze-thaw (one cycle: -20°C and 25°C each for 24 h). Various stability-indicating parameters, such as colloidal dispersion stability (Zavg, PDI, and ZP), physical properties (color, pH, RI, structural integrity/ optical microscopy, sedimentation, precipitation, and phase separation), chemical properties (FTIR), and pharmaceutical properties (% EE, % LC, and flexibility) were accessed intermittently and at the end of the study. In addition, the lyophilization stability was evaluated for the possible change in colloidal and pharmaceutical properties. Briefly, the freshly prepared optimized TFs were subjected to pre-freezing at -20°C overnight followed by lyophilization in a lyophilizer (LFD-BT-101, Labocon Scientific Limited, UK). The Zavg, PDI, and ZP were accessed after reconstitution with water by slight agitation.

### In-vitro cytotoxicity assay

Melanoma cell line (B16F10) and human embryonic kidney 293 cells (HEK 293) were obtained from the National Centre for Cell Science (NCCS), Pune, India. The MTT assay was performed for the in-vitro cytotoxicity of optimized TFs formulation along with unformulated PLFEE extract as per our reported method with certain modifications [4]. The B16F10 and HEK 293 were seeded at a concentration of 1 × 106 cells/well in a microtiter plate, containing DMEM/F-12 medium with 10% FBS, 50 unit/mL penicillin, and streptomycin, and incubated in 5% CO2 atmosphere for 24 h at 37°C to attain 70% of confluency. Due to the hydrophobic nature of PLFEE, it was solubilized in 0.2% DMSO for treatments. After the attainment of confluency, the medium was discarded, washed thrice with phosphate-buffered saline (PBS, 10 mM, pH 7.4), and further incubated with serum-free fresh media containing various concentrations of test substances (optimized TFs and PLFEE extract) and negative control (placebo optimized TFs and 0.2% DMSO) for 24 h. Then the sample solutions were substituted with serum-free media containing 200 μL of MTT solution (5 mg/mL), and cells were further incubated for 4 h at 37°C. The previous medium was removed, and the cells were washed thrice with PBS. The formazan crystals generated from MTT reduction by viable cells were dissolved by the addition of 150 µL of DMSO. Then the absorbance of the solution was measured at 570 nm in a microtiter plate reader (Bio-Rad Laboratories, Munchen, Germany). The percentage cell viability was calculated using the formula in Equation S8.

% cell viability=Abs(t)Abs(C)×100                                                       (Eq. S8)

where Abs(t) and Abs(c) are the absorbances of the plate with the treated sample and the absorbance of the control (without any treatment) respectively. The concentration required for 50 % inhibition of cell viability (IC50 value) was calculated using nonlinear regression analysis of log (concentration) vs. response data by GraphPad Prism 5 Software (GraphPad Software, Inc., San Diego, California). The % B16F10 cell viability at each concentration of free neat PLFEE and optimized TFs were compared using paired student t-test at a 95% level of significance.

### In-vitro cellular uptake study

To examine whether the TFs can be internalized by the B16F10 cells, the uptake of Coumarin 6 (CU-6)-loaded TFs was investigated. CU-6, a hydrophobic fluorescent dye, was used as a green fluorescent marker to track the TFs within the cancer cells. The CU-6 (1.2 mg) loaded TFs were formulated in a dark environment in a similar processing condition as that of the optimized TFs by replacing standardized PLFEE with CU-6 (for its loading in TFs, the CU-6 was solubilized in chloroform instead of ethanol as in case of PLFEE). B16F10 cell line cells were seeded into a 12-well culture plate at 1 × 105 cells per well and similarly incubated for 24 h as done for the MTT assay. After incubation, the cells were treated with media containing free CU-6 (0.055 µg/mL) and an equivalent amount of CU-6-loaded TFs and further incubated for 1 h at 37°C. The used medium, along with the treatments, was removed by washing cells with 1 mL PBS. After paraformaldehyde fixing, staining with 4′,6- diamidino-2-phenylindole (DAPI) was done for 15 min. Then, cancer cells were photomicrographed by a fluorescence microscope EVOS FLC Invitrogen fluorescence microscope (Life Technologies) at the UV excitation wavelength. The quantitative assessment of green fluorescence (i.e., total “area” and mean “gray” value) due to the free CU-6 and CU-6-TFs was carried out by processing the photomicrographs via ImageJ software. An unpaired student t-test was used to compare the results at a 95% confidence level.

## Formulation of transferosomal gel (TFG) or transgelosome, placebo TFG, and plain gel

The TFG was prepared by incorporating the optimized TFs (containing 250 mg of PLFEE) into the Xanthan gum-based gel. Placebo TFG containing placebo-optimized TFs and plain gel containing standardized PLFEE and a were formulated for comparison purposes. Based on preliminary studies on the rheology, consistency, and spreadability of TFG and its comparison with the marketed gel (Omnigel, Cipla Ltd.), the percentage of the gelling agent was fixed.  For TFG preparation, the Xanthan gum was gently dispersed portion-wise to the TFs formulation under continuous stirring. Propylene glycol (PG) was used as a humectant. Preservatives, such as methylparaben and propylparaben were added one by one, mixed properly, and allowed to hydrate the gel for 24 h. The placebo TFG was formulated similarly by incorporating placebo-optimized TFs into the gel and adding the remaining additives. The plain gel was prepared by directly incorporating the equivalent amount of PLFEE into a hydrated Xanthan gum-gel base, followed by the addition of humectant and preservatives.  All the gel products were kept individually in screw-capped glass containers.

## Evaluation of TFG

### Organoleptic properties

The color and appearance were observed visually.

### Consistency and homogeneity

The consistency and homogeneity of the prepared gel formulations were inspected by visual observation,  graded as +++ (Good), ++ (Fair), + (Poor) [5], and compared with the marketed gel (Omnigel, Cipla Ltd.). A small amount of each gel was placed between the thumb and the index finger, slightly rubbed, and evaluated for consistency and the existence of any masses or lumps [6].

### Spreadability and extrudability

Accurately 0.5 g of gel was placed within a circle of 1 cm diameter pre-marked on a glass plate, a second plate (4 mm thick) was placed over it, and a weight of 500 g is kept on it for 5 min. The increase in diameter due to the spreading of gel was traced by marker and a minimum of 3 diameters was measured, and the average was calculated. The experiments were repeated in triplicate, and the results were presented as the average of three measurements [6, 7]. Extrudability in terms of weights needed to extrude a 0.5 cm ribbon of gel from a collapsible aluminum tube in 10 seconds was calculated [8].

### pH

A 10% w/v dispersion of TFG, placebo gel, and the plain gel was made with double distilled water, and the pH was evaluated using a digital pH meter (PC 700, Eutech Instrument, Singapore) which was previously calibrated with pH 4, pH 7 and pH 10 buffer solutions [9]. All the measurements were performed in triplicates at room temperature, and average values were reported.

### Rheological Studies

The rheology of gel formulations was studied by Anton Paar parallel plate rotational rheometer (MCR 72, Anton Paar GmbH, Austria) equipped with a 25 mm spindle and RheoCompassTM software (version: 1.3). The rheology was studied at a constant shear rate (γ’ = 50 1/s), increasing shear rate (γ’= 0.1 to 100 1/s), and amplitude sweep (γ = 0.01 to 100%, ω = 10 1/s) mode.  About 0.5 g of the gel was placed between plates, and the analysis was performed by maintaining a 1 mm gap between the plates at 25 ± 1°C in triplicates. After each measurement, the plate was cleaned and dried properly.

### Drug content and content uniformity determination

The drug content of TFG and the plain gel was determined by the validated HPLC method. Briefly, 200 mg of each gel was diluted with 5 mL HPLC grade methanol, vortexed, bath sonicated, centrifuged at 10000 rpm for 10 min, filtered through 0.22 µm syringe filter, and the PIP content was analyzed using the validated HPLC method. The content uniformity of each gel was estimated by quantifying the PIP content in samples taken from four different regions of the container.

### Syneresis

Accurately 200 mg of TFG, plain gel, and placebo TFG were placed individually in 2 mL of microcentrifuge tube (Eppendorf, Germany), weighed, centrifuged (10 min at 10000 rpm), and the supernatant fluid (phase separated) was discarded. The tubes were reweighed, and the percentage syneresis was calculated using Equation S9.

% syneresis=W1-W2W1                                                                                      (Eq. S9)

Where, W1 is the weight of the tube with gel before centrifugation, and W2 is the weight after centrifugation followed by decanting the fluid.

### Compatibility study

The drug-excipient compatibility of the gel formulations was investigated by ATR-FTIR spectroscopy by comparing individual formulation components, physical mixture, and formulations similarly as stated under the compatibility study in TFs. To avoid the dominating broad peak due to water, the hydrogels were freeze-dried for 12 h before ATR-FTIR analysis.

### In-vitro drug release and release kinetics

The in-vitro drug release with respect to PIP from the TFG-F2, plain gel, optimized TFs formulation, and PLFEE solution (in media) was carried out by the dialysis bag method. The seamless cellulose dialysis tubing (Dialysis Membrane-70, MWCO 12000-14,000 Daltons, pore size: 2.4 nm, average flat width - 28.46 mm, average diameter- 17.5 mm, capacity approx. - 2.41 mL/cm, Himedia, Laboratories, Pvt. Ltd., Mumbai, India) was soaked overnight in deionized water to remove the preservatives and to swell the bag. Phosphate buffered saline (PBS pH=7.4) containing 0.5% of T-80 was used as release media for in-vitro release study [10]. Accurately 25 mg of PLFEE in solution form (in release media), an equivalent amount of optimized TFs, plain gel, and TFG-F2 were taken in a dialysis bag, hermetically sealed at both ends by threads and placed into a beaker containing 80 mL of release media. The receptor medium was maintained at 37 ± 0.5°C with continuous stirring at 150 rpm by a temperature-controlled magnetic stirrer with a hot plate (IKA C-MAG HS 7). At predetermined time intervals (0, 0.083, 0.25, 0.5, 0.75, 1, 2, 3, 4, 5 6, 8, 10, 12, 14, 16, 18, 20, 22, 24, 26, 28, 30, 32, 34, 36, 38, and 48 h), 1 mL of the aliquot was withdrawn from receptor medium and immediately replenished with the same volume of fresh blank medium to maintain sink condition. The amount of drug released was estimated by the validated HPLC method. The results were expressed in terms of the cumulative percentage of PIP released as a function of time.

The data of the in-vitro drug release study was fitted to various mathematical kinetic models (zero order, first order, Korsmeyer-Peppas, Higuchi, and Hixson-Crowel cube root) to predict the release kinetics of PIP from TFs formulation. The linear regression analysis was performed to analyze the release data, and the correlation coefficient (R2) in each case was estimated to predict the best-fitting model.  The mechanism of drug release was investigated by fitting the 1st 60% of the in-vitro drug release data to the Korsmeyer-Peppas model and estimating the release exponent (n). The following mathematical models are used for kinetic analysis.

Zero-order kinetics, C0 -Ct =K0 t                                               (Eq. S10)

Where C0, Ct, and K0 are the drug concentration at time (t = 0), drug released at time t, and zero-order release constant.

First-order kinetics, LogC=LogC0-K1 t 2.303                     (Eq. S11)

Where C is the % drug remaining at time t, C0 is the initial drug concentration and K1 is the first-order rate constant.

Higuchi model, Q=KHt1/2                                                              (Eq. S12)

Where Q is the quantity of drug released at time t and KH is the Higuchi constant.

Korsmeyer-Peppas model, MtM∞=kkptn                                            (Eq. S13)

Where Mt is the quantity of drug released at time t, M∞ is the quantity of drug released at ∞ time, Mt / M∞ is the fraction of drug released at time t, kkp is the Korsmeyer rate constant, and n is the diffusional exponent.

Hixson-Crowel cubic root law, 3W0-3Wt=KHCt                                  (Eq. S14)

Where W0 is the initial amount of the drug (amount of drug remaining at time 0), Wt is the amount of drug remaining to be released at time t, and KHC is the Hixson-Crowell rate constant.

### Stability Studies

The stability testing was carried out as per ICH guidelines (ICH Q1 R2). The gel formulations were filled in the sterile collapsible aluminum tubes and subjected to long-term stability conditions (5 ± 3°C) for 12 months and accelerated conditions (25 ± 2°C/60 ± 5% RH) for 6 months. Periodically at 0, 6, 9, and 12 months for long-term stability study and 0, 3, and 6 months for accelerated condition, the formulations were evaluated for organoleptic properties, consistency, homogeneity, spreadability, extrudability, pH, viscosity, drug content, syneresis, and drug-excipient compatibility.

## Animal experiments

The guidelines of the “Committee for the Purpose of Control and Supervision of Experiments on Animals” (CPCSEA) were strictly followed for care and animal experiments. The experiments were carried out following an approved protocol from Institutional Animal Ethics Committee (IAEC Approval Number: IIT(BHU)/IAEC/2022/001). Female C57BL/6 mice: 7-8 weeks old, 18 ± 1.865 g body weight) were housed in cages with free access to standard food (Laboratory animal feeds, VRK Nutritional Solutions, Maharashtra, India) and water. All the animals were kept in a room (25 ± 1°C, 55 ± 5% RH) with 12 h of dark/light cycle and accustomed to the laboratory conditions over 1 week before experiments.

### Ex-vivo skin permeation study and permeability kinetics

The skin of C57BL/6 female mice was collected from the healthy group of the dermal toxicity study. The skin permeability study was carried out by OECD 428 guidelines (in-vitro skin absorption). To investigate the in-vitro transdermal permeability of a drug, a nonoccluded open skin hydration setup was followed to maintain a transepidermal aqueous gradient that acts as a driving force for the skin penetration of transfersomes [11]. The hair from the dorsal side was removed precisely using an electric clipper, the skin was isolated, and the adhering fatty material was removed by isopropyl alcohol using a cotton swab. The skin was wrapped in aluminum foil, and stored at - 20°C until further use. The stored skin was thawed to room temperature, and hydrated with water for 2 h to attain the equilibrium. The ex-vivo skin permeability was carried out using a vertical Franz diffusion cell (Kshitij International Equipment, India) with a 20 mL receptor volume and diffusional area of 2.545 cm2. The skin was sandwiched between the donor and receptor compartments with the epidermis towards the donor compartment and exposed to the receptor compartment containing fresh phosphate-buffered saline (pH 7.4 containing 0.5% T-80). Sodium azide (0.0025% w/v) was added to the medium to avoid the growth of microbes [12]. The receptor media was stirred continuously at 150 rpm using temperature controlled magnetic stirrer (IKA C-MAG HS 7, IKA, Germany), and the temperature of the receptor compartment was maintained at 37 ± 1°C to achieve the physiological skin temperature of 32 ± 1°C [13]. The 4.658 mg PLFEE containing plain gel (0.2 g) and an equivalent amount of TFG-F2 (0.218 g) formulations were applied to the skin uniformly. Aliquots of 1 mL were collected at regular intervals (0, 0.083, 0.25, 0.5, 1, 2, 3, 4, 5 6, 8, 10, 12, 14, 16, 18, 20, 22, 24, 26, 28, 30, 32, 34, 36, and 38 h) from receptor compartment and replenished with the same volume of fresh release medium to maintain the sink condition. Collected samples were diluted with suitably with HPLC grade methanol, centrifuged, filtered through the 0.22 μM membrane filter, and the supernatant was analyzed for the drug permeated by validated HPLC method. The cumulative amount of PIP permeated through a unit area of skin at a predetermined time was calculated using Equation S15 [14].

Cumulative amountQi=Ci V+1i-1Ci-1×ViA                                                   (Eq. S15)

Where, where Qi is the cumulative amount of drug permeated through the skin, A is the effective diffusional area (2.545 cm2); V represents the volume of the receptor medium (20 mL); Ci represents the drug concentration at a predetermined time (i) in receptor medium, Vi represents the volume after each sampling time; 1i-1Ci-1 denotes the summed total of the previously measured concentrations. The permeability results were kinetically analyzed by various mathematical models as described in in-vitro release study.

The permeability coefficient (kp) was calculated using Equation S16 [15].

Permeability coefficient (kp)=dQdtA.Cd                                          (Eq. S16)

Where, A is diffusion area, dQ/dt = amount of drug/time, and Cd is the drug concentration in the donor compartment

The drug permeation rate (flux) at steady state (Jss) was calculated by dividing the slope of the linear portion of the graph by the area of the diffusion cell (Equation S17) [16].

Steady state Flux Jss=dQdtA= kp×Cd                                          (Eq. S17)

Where, dQ/dt is the slope of the linear portion, and A is the diffusion area.

The maximum flux (Jmax) was calculated using Equation S18.

Maximum Flux Jmax=dQdtmaxA                                          (Eq. S18)

Where, dQ/dtmax represents the maximum amount of drug permeated at the end of the study and A is the diffusional area.

The enhancement ratio (Er) was estimated using Equation S19 [16].

Enhancement ratio Er=Jss of Transgelosome Jss of Control Gel                                          (Eq. S19)

### Depth of skin penetration via Confocal laser scanning microscopy (CLSM) microscopy

CLSM was used to study the depth of permeation of plain gel and TFG F2 across the skin using CU-6 as a fluorescent marker in place of standardized PLFEE. Each formulation was applied nonocclusively to the dermal side of the C57BL/6 mice skin and subjected to the vertical diffusion apparatus similarly (as in the case of ex-vivo permeability study) for 8 h.  Then, the skin samples were removed carefully and washed thrice in running tap water to remove sample residue. The skin samples from the diffusion area were carefully removed and optically scanned and sliced (12 μM thickness) by the Z-stacking option of a confocal laser microscope (CLSM 900, Carl Zeiss Microscopy, GMBH, Germany), using an argon beam at an excitation wavelength of 457 nm.  The photomicrographs were captured using Zen (Blue edition) software (version: 3.6). All the system parameters were kept constant during the measurements to compare the photomicrographs.

### Acute dermal toxicity and skin irritation study

Acute dermal toxicity study of standardized PLFEE was carried out on nulliparous and non-pregnant C57BL/6 female mice (8-9 weeks old, 20 ± 1.573 g body weight) as per Organization for Economic Co-operation and Development (OECD) 402 guideline (Acute Dermal Toxicity: Fixed Dose Procedure). The dermal toxicity of the standardized PLFEE was investigated by conducting “range-finding study’ followed by “main study”. Prior to the toxicity study, the mice were caged individually to avoid oral ingestion of the test sample by other animals in the cage. All fur from the dorsal region (~ 10% of the total body surface area) of C57BL/6 mice was removed by clipping before topical application with special attention to avoid abrading the skin. For better contact with the skin, the dried PLFEE was slightly moistened with distilled water. A starting dose (200 mg/kg) of the standardized PLFEE followed by 1000 mg/kg, and 2000 mg/kg was uniformly applied topically as a very thin layer on a single animal/group in the range-finding study followed by repeating the aforementioned doses on 2 animals/ group in the main study. For statistical analysis, the obtained final safe dermal dose was applied to 4 animals/group. The animals topically applied with distilled water served as a control group for comparison purposes. The prolonged (24-h) skin retention of standardized PLFEE and avoidance of ingestion by the animals was ensured by means of a porous gauze dressing.  Each animal was carefully observed initially just after administration, after the first 30 min, with special attention at first 2-6 h, periodically during the first 24 h, and daily afterward for up to 14 days for detecting any sign of toxicity (changes in skin, fur, eyes, mucous membranes), survival or behavioral, and body weight changes.  At the end of the exposure period (24 h), the residual standardized PLFEE was removed. The treatment site was thoroughly observed at 24, 48, and 72 h after the removal of the test chemical using the Draize criteria. After 14 days, the mice were thoroughly observed, weighed, anesthetized with isoflurane, and blood was collected by cardiac puncture for hematological and biochemical studies as per the manufacturer’s instructions.

Then the animals were humanly sacrificed, and the vital organs (heart, liver, kidney, spleen, and lungs) were carefully isolated, washed with ice-cold phosphate-buffered saline, and stored in 10% aqueous formalin for 12 h for histopathological studies. Paraffin organ sections (~ 4 μm thick) were cut and stained with eosin and hematoxylin and mounted in a non-aqueous mounting medium (Dibutylphthalate Polystyrene Xylene (DPX)). The photomicrographs of the sections were captured at 10x magnification using a light microscope (Magnus MLX Plus, Olympus Opto Systems India Pvt. Ltd., Uttar Pradesh, India) furnished with a digital microscopic camera (Magcam DC 5, 5.1 MP) and Magvision software (version: x36, 3.7.6820). Based on all the observations, the dermal toxicity of standardized PLFEE was reported as per Globally Harmonised System (GHS) category (category 1- 5/Unclassified).

The Draize patch test was used to assess the skin irritation potential of prepared gel formulations. Briefly, the study was performed on female C57BL/6 mice (20 ± 1.471 g body weight). Carefully 10% of hair was removed from the dorsal side by an electric clipper 24 h before the test, washed with distilled water, and applied uniformly with 0.5 g of placebo TFG-F2 (vehicle control), TFG-F2, plain gel, and aqueous formalin solutions (0.8% v/v) as a positive control. The skin surface was inspected for signs of erythema and edema at 24, 48, and 72 h after application. The responses were examined as reactions on the skin surface, the scores in terms of “primary irritation index (PII)” were assigned, and the irritability potential of the formulations was interpreted using the “Grading values and response categories table” (Table S15).

## In-vivo anticancer activity in melanoma (B16F10) bearing C57BL/6 mice

The in-vivo anticancer activity was investigated in solid tumor/melanoma (B16F10) bearing C57BL/6 female mice (8-9 weeks old, 20 ± 1.324 g body weight)).  The C57BL/6 mice were kept in cages, with free access to food and water, and maintained under controlled environmental conditions on a 12 h dark/light cycle in a room at 22 ± 3°C and 55 ± 5% RH. The hair from the dorsal side was carefully removed with an electric clipper prior to the tumor induction. The syngeneic transplantation model was utilized for developing solid tumors in female C57BL/6 mice using murine melanoma cells (B16F10).  The murine melanoma cells (B16F10) were collected from National Centre for Cell Sciences (NCCS; Pune, India) and grown in DMEM/F-12 media containing 10% fetal bovine serum (FBS) and antibiotics (penicillin and streptomycin solution, 50 unit/mL) at 37°C in a 5% CO2 incubator (Heracell VIOS 160i, Thermo Fisher, USA). The cells were grown in T75 Flasks (Thermo Fisher Scientific, USA) up to 90% confluency and harvested by trypsinization (using trypsin: EDTA at 0.05:0.03 w/v) followed by centrifugation (5000 rpm), washing, and pellet dispersion in phosphate-buffered saline (PBS, pH 7.4).  For solid tumor development, the cells were adjusted to 1×106 cells/0.1 mL in PBS, and accurately 100 μL of the cell suspension was injected subcutaneously into the dorsal side of C57BL/6 mice. After 7 to 8 days, mice bearing palpable tumor (volume: 35 ± 3 mm3) were topically applied with a placebo gel, plain gel (at a dose of 200 mg/kg PLFEE), and an equivalent quantity of TFG-F2 daily up to 30 days. Dacarbazine (DTIC) as a standard anticancer drug, was administered at a dose of 5 mg/kg intraperitoneally (i.p.) every 2 days for up to 30 days [17]. The treatments comprising DTIC with standardized PLFEE-loaded plain gel or TFG-F2 were also provided to evaluate their efficacy as supportive therapy. Body weight and tumor size were evaluated throughout the treatment period.

### Experimental design

A total of 35 adult female C57BL/6 mice (weighing 21 ± 1.665 g, 9-10 weeks old) were divided into 7 groups as follows:

- Group-I (Normal control): Non-tumor-bearing mice

- Group-II (Tumor control): Tumor-bearing mice, topically applied with placebo gel (0.196 g/ animal) daily

- Group-III (Standard drug/ DTIC group): Tumor-bearing mice, receiving DTIC (5 mg/kg) i.p. every 2 days.

- Group-IV (PLFEE-loaded plain gel group): Tumor-bearing mice, applied with standardized PLFEE-loaded plain gel (0.180 g/animal, at a dose of 200 mg/kg) daily

- Group-V (PLFEE-loaded Transgelosome group): Tumor-bearing mice, applied with standardized PLFEE-loaded transgelosome (0.196 g i.e., equivalent to 0.180 g of plain gel/animal, at a dose of 200 mg/kg) daily

- Group-VI (DTIC + PLFEE loaded plain gel group): Tumor-bearing mice applied with standardized PLFEE loaded plain gel (0.180 g/animal) daily and DTIC (5 mg/kg b.wt.) i.p. every 2 days.

- Group-VII (DTIC + Transgelosome group): Tumor-bearing mice, applied with standardized PLFEE loaded transgelosome (0.196 g/animal) daily, and DTIC (5 mg/kg b.wt) i.p. every 2 days.

### Tumor regression analysis

The tumor regression analysis was carried out as per the reported protocol [18].

#### Tumor volume (TV):

The size of the solid tumor was measured during the treatment using digital Vernier calipers (ZHART, CT-ZT-VERNIER, India) and the tumor volume was calculated by using Equation S20.

TV=length×width22                                            (Eq. S20)

#### Volume doubling time (VDT):

VDT was calculated from the time required for the solid tumor to achieve double the initial volume.

#### Tumor growth inhibition (% TGI):

It was calculated at the end of the study using Equation S21.

% TGI=1-(TtT0×C0Ct)1-C0Ct  ×100                             (Eq. S21)

Where Tt and T0 are the median tumor volume of treated at time t, and time 0, respectively. Ct and C0 are the median tumor volume of control at time t, and time 0, respectively. Tumor growth inhibition greater than 50% is considered meaningful.

#### Tumor weight and Histopathology

At the end of the study, mice from each group were sacrificed by cervical dislocation for tumor weight and histopathology studies. Tumors from various groups were collected, weighed, fixed in 10% buffered formalin for 12 h, and similarly processed for histopathology as described in the acute toxicity study.

## Statistical analysis

The mean and standard deviation (SD) for all experiments were calculated and expressed as mean ± SD. Statistical analysis was performed by one-way analysis of variance (ANOVA) followed by Tukey’s test (for 3 groups or more) or students t-test (between two groups) at p<0.05 using GraphPad Prism 5 (GraphPad Software, Inc., San Diego, California).

# Results

## Validation of the HPLC method

The HPLC chromatograms of PIP and PLGN are shown in Figure S1A and Figure S1B, respectively. The respective inset figures showed the calibration curves. Table S1 and Table S2 showed the complete validation data of the HPLC method for the quantification of PIP and PLGN, respectively.

Figure S1 HPLC chromatograms of PIP and PPLGN each of 28 µg/mL (A) Chromatogram of PIP (Rt = 7.087 ± 0.053 min) at λmax of 342 nm with the inset figure showing the calibration curve for PIP, (B) Chromatogram of PLGN (Rt = 6.413 ± 0.014 min) at λmax of 340 nm with the inset figure showing the calibration curve for PLGN

HPLC: High performance liquid chromatography; PIP: Piperine; PLGN: Piperlonguminine; Rt: Retaintion time

Table S1 Summary of validated HPLC method for estimation of PIP

| Parameters | Values | % RSD |
| --- | --- | --- |
| Linearity and range |  |  |
| Regression equation | y = 276947.424 x - 200378.812 |  |
| Correlation coefficient (r2) | 0.997 |  |
| Range | 2 to 30 µg/mL |  |
| Accuracy |  |  |
| 50% level | 99.85 | 0.757 |
| 100% level | 101.031 | 1.694 |
| 150% level | 99.345 | 1.242 |
| Precision |  |  |
| Repeatability (12 µg/mL) | 3230831.167 ± 5177.835 m.A.U. | 0.16 |
| Intermediate precision |  |  |
| Intra-day |  |  |
| 6 µg/mL | 1618408 ± 3798.53 m.A.U. | 0.234 |
| 12 µg/mL | 3241725.333 ± 4740.057 m.A.U. | 0.146 |
| 18 µg/mL | 4714037.333 ± 14102.094 m.A.U. | 0.299 |
| - Inter-day |  |  |
| 6 µg/mL | 1622421 ± 5989.94 m.A.U. | 0.369 |
| 12 µg/mL | 3256179.333 ± 10828.978 m.A.U. | 0.332 |
| 18 µg/mL | 4707917 ± 12164.467 m.A.U. | 0.258 |
| LOD | 0.259 μg/mL |  |
| LOQ | 0.786 μg/mL |  |
| Robustness |  |  |
| - Flow rate |  |  |
| 0.8 mL/min | 4190108.667 ± 8244.626 m.A.U. | 0.196 |
| 1 mL/min | 3223921.667 ± 4744.925 m.A.U. | 0.147 |
| 1.2 mL/min | 2833650.333 ± 12476.467 m.A.U. | 0.44 |
| - Mobile phase composition (Methanol: Water) |  |  |
| 78:22 v/v | 3450097 ± 13660.3214 m.A.U. | 0.395 |
| 80:20 v/v | 3257255 ± 42512.258 m.A.U. | 1.305 |
| 82:18 v/v | 3459427.66 ± 25292.359 m.A.U. | 0.731 |
| - Run time |  |  |
| 8 min | 3382801.333 ± 11055.37 m.A.U. | 0.326 |
| 10 min | 3227710 ± 501.352 m.A.U. | 0.015 |
| 12 min | 3375691.667 ± 16612.698 m.A.U. | 0.492 |
| - Wavelength |  |  |
| 340 nm | 3390391.333 ± 20376.823 m.A.U. | 0.601 |
| 342 nm | 3377712 ± 19944.805 m.A.U. | 0.59 |
| 344 nm | 3340953.333 ± 19354.762 m.A.U. | 0.579 |
| System suitability study |  |  |
| Area | 3230831.167 ± 5177.835 m.A.U. | 0.16 |
| Retention time (Rt) | 7.047 ± 0.023 min | 0.425 |
| Number of theoretical plates | 3592.834 ± 43.26 | 1.204 |
| Peak purity | 0.998 ± 0.002 | 0.2 |
| Tailing factor (Asymmetry) | 0.9235 ± 0.0017 | 0.194 |
| Capacity factor (k1) | 1.448 ± 0.009 | 0.646 |

Table S2 Summary of validated HPLC method for estimation of PLGN

| Parameters | Values | % RSD |
| --- | --- | --- |
| Linearity and range |  |  |
| Regression equation | y = 349329.568 x - 272061.184 |  |
| Correlation coefficient (r2) | 0.996 |  |
| Range | 2 to 30 µg/mL |  |
| Accuracy |  |  |
| 50% level | 105.986 | 0.425 |
| 100% level | 99.976 | 0.201 |
| 150% level | 100.268 | 1.241 |
| Precision |  |  |
| Repeatability (12 µg/mL) | 3643443.167 ± 4354.112 m.A.U. | 0.119 |
| Intermediate precision |  |  |
| - Intra-day |  |  |
| 6 µg/mL | 1880619 ± 1216.598 m.A.U. | 0.064 |
| 12 µg/mL | 3687662.667 ± 32458.115 m.A.U. | 0.88 |
| 18 µg/mL | 5872113.333 ± 22782.816 m.A.U. | 0.387 |
| - Inter-day |  |  |
| 6 µg/mL | 1850762.667 ± 13350.252 m.A.U. | 0.721 |
| 12 µg/mL | 3639347.333 ± 37043.657 m.A.U. | 1.017 |
| 18 µg/mL | 5845683.333 ± 9105.994 m.A.U. | 1.155 |
| LOD | 0.27 μg/mL |  |
| LOQ | 0.819 μg/mL |  |
| Robustness |  |  |
| - Flow rate |  |  |
| 0.8 mL/min | 4657913 ± 41988.913 m.A.U. | 0.901 |
| 1 mL/min | 3655028 ± 19590.404 m.A.U. | 0.535 |
| 1.2 mL/min | 3157162.333 ± 11512.149 m.A.U. | 0.364 |
| - Mobile phase composition (Methanol: Water) |  |  |
| 78:22 v/v | 3775809 ± 13947.62 m.A.U. | 0.369 |
| 80:20 v/v | 3642568 ± 32103.463 m.A.U. | 0.881 |
| 82:18 v/v | 3785191.667±22562.0006 m.A.U. | 0.596 |
| - Run time |  |  |
| 8 min | 3746709.667 ± 55753.844 m.A.U. | 1.488 |
| 10 min | 3644321.667 ± 5695.461 m.A.U. | 0.156 |
| 12 min | 3716112 ± 54328.062 m.A.U. | 1.461 |
| • Wavelength |  |  |
| 340 nm | 3711673.667 ± 43144.199 m.A.U. | 1.162 |
| 342 nm | 3688361.33 ± 66729.35 m.A.U. | 1.809 |
| 344 nm | 3856646 ± 17489.522 m.A.U. | 0.453 |
| System suitability study |  |  |
| Area | 3643443.167 ± 4354.112 m.A.U. | 0.119 |
| Retention time (Rt) | 6.406 ± 0.041 min | 0.646 |
| Number of theoretical plates | 3541.5 ± 31.17 | 0.88 |
| Peak purity | 0.99 ± 0.007 | 0.775 |
| Tailing factor (Asymmetry) | 0.868 ± 0.007 | 0.838 |
| Capacity factor (k1) | 1.135 ± 0.002 | 0.193 |

## Formulation development of transferosome and flexibility analysis

The detailed formulation methodology and various TFs batches are shown in Figure S2, and Figure S3, respectively.

Figure S2 Formulation methodology of standardized PLFEE-loaded TFs by thin film hydration method

PLFEE: P. longum fruits ethanolic extract; TFs: transferosome

Figure S3 Twenty formulations of standardized PLFEE-loaded TFs as per the design of the experiment

PLFEE: P. longum fruits ethanolic extract; TFs: transferosome

Figure S4 In-house fabricated device for the flexibility determination of TFs

TFs: Transferosome

The levels of three independent variables and the response as per the CCD model are displayed in Table S3.

Table S3 Coded levels, real values of each factor, and Critical Quality Attributes (CQA)

|  | Levels |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Coded Values |  |  |  |  |
|  | -1.681 | -1 | 0 | +1 | +1.681 |
| Independent variables (CMAs and CPP) | Real values |  |  |  |  |
| Phospholipon® 90 H (X1, mg) | 315.91 | 350 | 400 | 450 | 484.089 |
| Tween® 80 (X2, mg) | 15.91 | 50 | 100 | 150 | 184.089 |
| Probe Sonication Time (X3, min) | 0.954 | 3 | 6 | 9 | 11.045 |
| Dependent variables (CQAs) | Goal |  |  |  |  |
| Vesicle Size (Y1, nm) | To minimize |  |  |  |  |
| Entrapment Efficiency (Y2, %) | To maximize |  |  |  |  |
| Flexibility (Y3, mL/s) | To maximize |  |  |  |  |

CQAs: critical quality attributes; CMAs: critical material attributes and CPP: critical process parameter

The results of chosen responses (Zavg (Y1), % EE (Y2), and flexibility (Y3)) with other evaluated parameters of each TFs are represented in Table S4.

Table S4 CCD-based TFs formulations with respective responses

|  | Factor 1 (X1) | Factor 2 (X2) | Factor 3 (X3) | Response 1 (Y1) | Response 2 (Y2) | Response 3 (Y3) | Other Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Formulation | A: Phospholipon 90 H (PL-90 H) | B: Tween® 80 | C: Probe Sonication Time | Vesicle Size (Zavg) | Entrapment Efficiency (EE) | Flexibility | Polydispersity Index (PDI) | Zeta Potential (ζ) | Loading Capacity (LC) | pH | Refractive Index (RI) |
|  | mg | mg | min | nm | % | mL/s |  | mV | % |  |  |
| 1 | 450 | 50 | 9 | 197.254 ± 3.215 | 86.545 ± 2.346 | 14.124 ± 2.245 | 0.211 ± 0.014 | -18.5 ± 0.275 | 9.606 ± 1.231 | 4.756 ± 0.012 | 1.335 ± 0.0001 |
| 2 | 450 | 50 | 3 | 231.253 ± 2.452 | 92.385 ± 3.457 | 13.254 ± 1.117 | 0.358 ± 0.006 | -17.8 ± 0.312 | 10.254 ± 1.543 | 4.743 ± 0.016 | 1.334 ± 0.0003 |
| 3 | 400 | 100 | 6 | 160.667 ± 3.554 | 62.846 ± 5.46 | 16.242 ± 2.623 | 0.184 ± 0.005 | -18.2 ± 0.242 | 6.975 ± 2.131 | 4.703 ± 0.024 | 1.337 ± 0.0004 |
| 4 | 350 | 50 | 9 | 110.334 ± 2.346 | 48.254 ± 4.489 | 14.215 ± 1.157 | 0.214 ± 0.014 | -11.8 ± 1.024 | 6.695 ± 1.546 | 4.81 ± 0.016 | 1.337 ± 0.0014 |
| 5 | 400 | 184.08975 | 6 | 129.334 ± 4.424 | 52.354 ± 3.247 | 12.213 ± 0.985 | 0.192 ± 0.048 | -17.2 ± 0.234 | 4.974 ± 3.071 | 4.733 ± 0.016 | 1.343 ± 0.0004 |
| 6 | 400 | 15.91035 | 6 | 171.667 ± 1.252 | 72.892 ± 1.278 | 10.244 ± 1.136 | 0.389 ± 0.006 | -18.2 ± 0.178 | 9.726 ± 1.067 | 4.52 ± 0.037 | 1.334 ± 0.0002 |
| 7 | 400 | 100 | 6 | 165.68 ± 2.246 | 65.254 ± 2.457 | 17.243 ± 2.016 | 0.237 ± 0.006 | -19.2 ± 0.123 | 7.243 ± 2.214 | 5.51 ± 0.035 | 1.338 ± 0.0003 |
| 8 | 400 | 100 | 11.0454 | 140.334 ± 3.423 | 56.235 ± 3.349 | 17.242 ± 0.896 | 0.201 ± 0.021 | -18.1 ± 1.214 | 6.242 ± 1.473 | 6.72 ± 0.016 | 1.34 ± 0.0007 |
| 9 | 484.09 | 100 | 6 | 238.333 ± 5.131 | 72.2865 ± 2.248 | 5.265 ± 1.273 | 0.128 ± 0.004 | -17.2 ± 0.542 | 6.868 ± 2.105 | 6.85 ± 0.028 | 1.337 ± 0.0008 |
| 10 | 400 | 100 | 6 | 161.213 ± 2.178 | 66.243 ± 4.478 | 16.242 ± 0.784 | 0.216 ± 0.024 | -19.4 ± 0.097 | 7.352 ± 1.136 | 4.78 ± 0.014 | 1.336 ± 0.0008 |
| 11 | 400 | 100 | 6 | 162.235 ± 1.546 | 63.234 ± 3.118 | 15.874 ± 0.858 | 0.221 ± 0.018 | -18.3 ± 0.132 | 7.018 ± 2.082 | 5.17 ± 0.008 | 1.335 ± 0.0001 |
| 12 | 315.91 | 100 | 6 | 75.5667 ± 2.147 | 38.152 ± 2.427 | 12.875 ± 1.346 | 0.216 ± 0.073 | -5.38 ± 0.245 | 5.091 ± 1.142 | 5.58 ± 0.021 | 1.334 ± 0.0001 |
| 13 | 350 | 150 | 9 | 97.1333 ± 3.279 | 45.545 ± 1.468 | 19.242 ± 1.023 | 0.183 ± 0.028 | -15.5 ± 0.312 | 5.055 ± 3.472 | 5.49 ± 0.008 | 1.335 ± 0.0002 |
| 14 | 400 | 100 | 6 | 167.548 ± 4.127 | 65.572 ± 3.314 | 16.124 ± 2.063 | 0.197 ± 0.029 | -19.2 ± 0.324 | 7.278 ± 2.140 | 4.79 ± 0.021 | 1.335 ± 0.0012 |
| 15 | 450 | 150 | 3 | 195.35 ± 2.179 | 66.356 ± 1.248 | 8.645 ± 0.965 | 0.276 ± 0.033 | -19.3 ± 0.547 | 6.137 ± 1.224 | 4.756 ± 0.012 | 1.338 ± 0.0003 |
| 16 | 400 | 100 | 6 | 168.235 ± 2.136 | 65.243 ± 1.118 | 16.578 ± 1.143 | 0.213 ± 0.028 | -17.2 ± 0.467 | 7.241 ± 0.985 | 4.756 ± 0.004 | 1.335 ± 0.0004 |
| 17 | 350 | 150 | 3 | 101.23 ± 1.746 | 65.246 ± 2.147 | 18.236 ± 2.034 | 0.249 ± 0.028 | -15.2 ± 0.247 | 7.242 ± 1.105 | 4.486 ± 0.055 | 1.337 ± 0.0002 |
| 18 | 400 | 100 | 0.954622 | 165.667 ± 3.364 | 80.324 ± 3.217 | 16.989 ± 0.864 | 0.401 ± 0.008 | -18.3 ± 0.176 | 8.915 ± 1.432 | 4.75 ± 0.008 | 1.337 ± 0.0002 |
| 19 | 350 | 50 | 3 | 120.243 ± 2.547 | 48.248 ± 2.211 | 8.345 ± 1.145 | 0.34 ± 0.042 | -9.32 ± 0.364 | 6.694 ± 2.017 | 4.63 ± 0.016 | 1.336 ± 0.0002 |
| 20 | 450 | 150 | 9 | 176.631 ± 1.578 | 42.213 ± 1.875 | 6.245 ± 1.368 | 0.212 ± 0.007 | -18.5 ± 1.081 | 3.904 ± 1.036 | 4.76 ± 0.018 | 1.335 ± 0.0001 |

Results were represented as mean ± standard deviation (n = 3)

CCD: Central Composite Design

## RSM and optimization of TFs

The statistical model fit summary of all responses is represented in Table S5.

Table S5 Statistical model fit summary

| Fit summary statistics: Vesicle Size (Y1) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Source (Models) | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² | R2 value | Std. Dev. | PRESS |  |
| Linear | <0.0001 | 0.0202 | 0.9677 | 0.9580 | 0.9728 | 7.63 | 1437.14 |  |
| 2FI | 0.1288 | 0.0287 | 0.9739 | 0.9579 | 0.9821 | 6.85 | 1439.42 |  |
| Quadratic | 0.0002 | 0.6756 | 0.9950 | 0.9892 | 0.9973 | 3.01 | 368.84 | Suggested |
| Cubic | 0.5261 | 0.6788 | 0.9947 | 0.9840 | 0.9983 | 3.08 | 546.14 | Aliased |
| Fit summary statistics: Entrapment Efficiency (Y2) |  |  |  |  |  |  |  |  |
| Source (Models) | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² | R2 value | Std. Dev. | PRESS |  |
| Linear | 0.0005 | 0.0001 | 0.6006 | 0.3786 | 0.6636 | 9.05 | 2419.08 |  |
| 2FI | <0.0001 | 0.0049 | 0.9174 | 0.8887 | 0.9435 | 4.11 | 433.45 |  |
| Quadratic | <0.0001 | 0.6796 | 0.9925 | 0.9847 | 0.9961 | 1.24 | 59.41 | Suggested |
| Cubic | 0.4899 | 0.9719 | 0.9924 | 0.9964 | 0.9976 | 1.25 | 13.98 | Aliased |
| Model summary statistics: Flexibility (Y3) |  |  |  |  |  |  |  |  |
| Source | Sequential p-value | Lack of Fit p-value | Adjusted R² | Predicted R² | R2 value | Std. Dev. | PRESS |  |
| Linear | 0.2254 | < 0.0001 | 0.0884 | -0.3209 | 0.2324 | 3.89 | 416.53 |  |
| 2FI | 0.0410 | 0.0001 | 0.3925 | 0.1731 | 0.5843 | 3.18 | 260.75 |  |
| Quadratic | <0.0001 | 0.1805 | 0.9766 | 0.9275 | 0.9877 | 0.6226 | 22.86 | Suggested |
| Cubic | 0.3877 | 0.0931 | 0.9787 | 0.3092 | 0.9933 | 0.5950 | 217.84 | Aliased |

The analysis of variance (ANOVA) outcomes of the statistical analysis by the Design-Expert software is represented in (Table S6).

Table S6 ANOVA for quadratic model and fit statistics for various responses

| ANOVA: Vesicle Size (Y1) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| Model | 34089.46 | 9 | 3787.72 | 417.79 | <0.0001 | significant |
| X1 | 30509.87 | 1 | 30509.87 | 3365.29 | <0.0001 |  |
| X2 | 1868.03 | 1 | 1868.03 | 206.05 | <0.0001 |  |
| X3 | 871.83 | 1 | 871.83 | 96.16 | <0.0001 |  |
| X1 X2 | 75.56 | 1 | 75.56 | 8.33 | 0.0162 |  |
| X1 X3 | 189.99 | 1 | 189.99 | 20.96 | 0.0010 |  |
| X2 X3 | 54.18 | 1 | 54.18 | 5.98 | 0.0346 |  |
| X1² | 83.96 | 1 | 83.96 | 9.26 | 0.0124 |  |
| X2² | 317.52 | 1 | 317.52 | 35.02 | 0.0001 |  |
| X3² | 209.20 | 1 | 209.20 | 23.07 | 0.0007 |  |
| Residual | 90.66 | 10 | 9.07 |  |  |  |
| Lack of Fit | 35.74 | 5 | 7.15 | 0.6507 | 0.6756 | not significant |
| Pure Error | 54.92 | 5 | 10.98 |  |  |  |
| Cor Total | 34180.12 | 19 |  |  |  |  |
| Fit statistics |  |  |  |  |  |  |
| Standard deviation (SD) | Mean | C.V (%) | R2 | Adjusted R2 | Predicted R2 | Adequate precision |
| 3.01 | 156.78 | 1.92 | 0.9973 | 0.9950 | 0.9892 | 74.6713 |
| ANOVA: Entrapment Efficiency (Y2) |  |  |  |  |  |  |
| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| Model | 3877.68 | 9 | 430.85 | 281.11 | <0.0001 | significant |
| X1 | 1386.66 | 1 | 1386.66 | 904.71 | <0.0001 |  |
| X2 | 601.21 | 1 | 601.21 | 392.25 | <0.0001 |  |
| X3 | 595.62 | 1 | 595.62 | 388.61 | <0.0001 |  |
| X1 X2 | 895.70 | 1 | 895.70 | 584.39 | <0.0001 |  |
| X1 X3 | 13.23 | 1 | 13.23 | 8.63 | 0.0148 |  |
| X2 X3 | 180.60 | 1 | 180.60 | 117.83 | <0.0001 |  |
| X1² | 163.59 | 1 | 163.59 | 106.74 | <0.0001 |  |
| X2² | 8.14 | 1 | 8.14 | 5.31 | 0.0439 |  |
| X3² | 22.45 | 1 | 22.45 | 14.65 | 0.0033 |  |
| Residual | 15.33 | 10 | 1.53 |  |  |  |
| Lack of Fit | 6.00 | 5 | 1.20 | 0.6439 | 0.6796 | not significant |
| Pure Error | 9.32 | 5 | 1.86 |  |  |  |
| Cor Total | 3893.01 | 19 |  |  |  |  |
| Fit statistics |  |  |  |  |  |  |
| Standard deviation (SD) | Mean | C.V (%) | R2 | Adjusted R2 | Predicted R2 | Adequate precision |
| 1.24 | 62.77 | 1.97 | 0.9961 | 0.9925 | 0.9847 | 61.7251 |
| ANOVA: Flexibility (Y3) |  |  |  |  |  |  |
| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| Model | 311.47 | 9 | 34.61 | 89.28 | <0.0001 | significant |
| X1 | 68.42 | 1 | 68.42 | 176.51 | <0.0001 |  |
| X2 | 2.41 | 1 | 2.41 | 6.23 | 0.0317 |  |
| X3 | 2.44 | 1 | 2.44 | 6.29 | 0.0310 |  |
| X1 X2 | 93.89 | 1 | 93.89 | 242.20 | <0.0001 |  |
| X1 X3 | 8.83 | 1 | 8.83 | 22.79 | 0.0008 |  |
| X2 X3 | 8.27 | 1 | 8.27 | 21.33 | 0.0010 |  |
| X1² | 87.84 | 1 | 87.84 | 226.61 | <0.0001 |  |
| X2² | 41.93 | 1 | 41.93 | 108.17 | <0.0001 |  |
| X3² | 2.03 | 1 | 2.03 | 5.25 | 0.0449 |  |
| Residual | 3.88 | 10 | 0.3876 |  |  |  |
| Lack of Fit | 2.73 | 5 | 0.5466 | 2.39 | 0.1805 | not significant |
| Pure Error | 1.14 | 5 | 0.2287 |  |  |  |
| Cor Total |  |  |  |  |  |  |
| Fit statistics |  |  |  |  |  |  |
| Standard deviation (SD) | Mean | C.V (%) | R2 | Adjusted R2 | Predicted R2 | Adequate precision |
| 0.6226 | 13.77 | 4.52 | 0.9877 | 0.9766 | 0.9275 | 30.6408 |

Figure S5 Diagnostic plots for response Y1 (A) normal plot of residuals, (B) Box-Cox plot, (C) predicted vs. actual plot, (D) residual vs. predicted plot, (E) residual vs. run, and (F) residual vs. factor plot

Y1: Vesicle Size (Zavg)

Figure S6 Diagnostic plots for response Y2 (A) normal plot of residuals, (B) Box-Cox plot, (C) predicted vs. actual plot, (D) residual vs. predicted plot, (E) residual vs. run, and (F) residual vs. factor plot

Y2: % Entrapment Efficiency (% EE)

Figure S7 Diagnostic plots for response Y3 (A) normal plot of residuals, (B) Box-Cox plot, (C) predicted vs. actual plot, (D) residual vs. predicted plot, (E) residual vs. run, and (F) residual vs. factor plot

Y3: Flexibility

Figure S8 Perturbation plots and overlay plot (A) perturbation plot for Y1, (B) perturbation plot for Y2, (C) perturbation plot for Y3, and (D) overlay plot indicating the optimized formula

Y1: Vesicle Size (Zavg); Y2: % Entrapment Efficiency (% EE); Y3: Flexibility

Table S7 represents the validations outcomes of the checkpoint batch.

Table S7 Validations results of checkpoint batch (n = 5)

| Responses | Predicted result | Experimental result | % Prediction error (% Bias) |
| --- | --- | --- | --- |
| Vesicle Size (Y1, nm) | 199.983 | 198.223 ± 1.701 | - 0.879 |
| Entrapment Efficiency (Y2, %) | 86.014 | 83.875 ± 1.602 | - 2.486 |
| Flexibility (Y3, mL/s) | 13.718 | 13.187 ± 0.544 | - 3.869 |

## Stability study of optimized TFs

The stability study results of optimized TFs were presented in Table S8.

### Physical stability

The results of physical stability represent no substantial changes in the physical properties under refrigerated conditions for up to 12 months. In contrast, the TFs showed slight sedimentation and phase separation after 6 months at accelerated stability conditions and the end of the heating-cooling cycle.

### Colloidal dispersion stability

The Zavg and PDI were found to be maintained for up to 6 months under refrigerated conditions and at the end of the freeze-thaw cycle, whereas it was found to be drastically increased with a lapse of time when evaluated under accelerated conditions and at the end of the heating-cooling cycle due to agglomeration of vesicles. Under long-term stability conditions (up to 9 months) and after the freeze-thaw cycle, the obtained PDI values are within 0.3, representing homogeneity; afterwards, the polydisperse vesicles were found.  In the case of long-term stability (up to 9 months) and at the end of the freeze-thaw cycle, the ζ on the TFs vesicles were found to be maintained and are within the range of ± 20-30 mV, representing moderately stable [4]. In contrast, under accelerated stability conditions and after the heating-cooling cycle, a substantial decrease in the ζ value was observed, ascribed to the agglomeration of vesicles, slight sedimentation, and phase separation.

### Pharmaceutical properties

The % EE, % LC, and flexibility were found to be slightly decreased while evaluated at 6 months under refrigerated conditions and at the end of freeze-thaw cycles. However, in the case of accelerated conditions and at the end of the heating-cooling cycle, the values were found to be drastically decreased which might be due to the aggregation, coalescence, and rupture of vesicles, leading to the formation of large-sized rigid multilamellar vesicles, loss of contained drug and flexibility.

### Chemical stability

The retention of all characteristic peaks of standardized PLFEE at the end of each stability study reflected no signs of chemical incompatibility.

### Lyophilization stability

The Zavg, PDI, and ZP after reconstitution of the lyophilized sample were found to be 198.357 ± 1.004 nm, 0.193 ± 0.002, and -23.14 ± 0.097 mV, respectively, which is close to the value of optimized TFs in liquid form, representing the lyophilization stability and long-term storage ability of the dried form. The % EE (86.359 ± 1.364 %) and LC (9.266 ± 0.643 %) were found to be close to the initial values, reflecting the lyophilization stability of the optimized TFs.

Table S8 Stability study of optimized TFs

| Parameters | Initial results | Long-term stability study (5°C ± 3°C) |  |  | Accelerated stability study (25°C ± 2°C/60% RH ± 5% RH) |  | Freeze-thaw (one cycle: -20 °C and 25 °C each for 24 h) and Heating-cooling cycle (one cycle: 40° C and 4° C each for 24 h) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 month | 6 months | 9 months | 12 months | 3 months | 6 months | Freeze-thaw cycle | Heating-cooling cycle |
| Color | Milky white | Milky white |  |  | Milky white |  | Milky white |  |
| pH | 4.756 ± 0.012 | 4.735 ± 0.038 | 4.894 ± 0.057 | 4.882 ± 0.044 | 4.772 ± 0.021 | 4.898 ± 0.057 | 4.822 ± 0.039 | 4.86 ± 0.015 |
| RI | 1.335 ± 0.0001 | 1.334 ± 0.003 | 1.335 ± 0.002 | 1.334 ± 0.007 | 1.335 ± 0.0001 | 1.334 ± 0.003 | 1.335 ± 0.002 | 1.335 ± 0.004 |
| Structural integrity | Spherical bilayered structure | Spherical bilayered structure |  |  | Spherical bilayered structure |  | Spherical bilayered structure |  |
| Sedimentation | No | No |  |  | No | Slight sedimentation | No | Slight sedimentation after 3nd cycle |
| Precipitation | No | No |  |  | No |  | No | No |
| Phase separation | No | No |  |  | No | Slight separation | No | Yes (after 3nd cycle) |
| Zavg (nm) | 196.368 ± 1.123 | 204.334 ± 1.368 | 221.56 ± 1.546 | 237.567 ± 2.357 | 228.327 ± 1.159 | 246.354 ± 2.374 | 197.616 ± 1.141 | 219.346 ± 2.352 |
| PDI | 0.185 ± 0.001 | 0.194 ± 0.004 | 0.284 ± 0.002 | 0.467 ± 0.004 | 0.335 ± 0.003 | 0.573 ± 0.004 | 0.187 ± 0.003 | 0.273 ± 0.004 |
| ζ (mV) | - 23.6 ± 1.355 | -22.13 ± 1.275 | -20.461 ± 0.873 | -17.462 2.32 ± 1.225 | -18.772 ± 1.053 | -15.357 ± 1.361 | -23.214 ± 0.996 | -17.354 ± 1.007 |
| EE (%) | 88.545 ± 2.134 | 85.463 ± 1.841 | 78.361 ± 2.134 | 73.253 ± 2.066 | 67.151 ± 2.165 | 53.243 ± 1.273 | 87.165 ± 2.263 | 77.434 ± 3.631 |
| LC (%) | 9.506 ± 0.223 | 9.171 ± 0.537 | 8.408 ± 0.667 | 7.860 ± 0.571 | 7.205 ± 0.356 | 5.712 ± 0.673 | 9.352 ± 0.584 | 8.308 ± 1.546 |
| Flexibility (mL/s ) | 13.719 ± 1.613 | 12.876 ± .0.542 | 10.572 ± 0.879 | 10.135 ± 0.753 | 9.152 ± 2.613 | 7.167 ± 0.786 | 12.435 ± 2.443 | 11.053 ± 0.873 |
| Drug-excipient compatibility | Compatible | Yes |  |  | Yes |  | Yes |  |
| Lyophilization stability |  |  |  |  |  |  |  |  |
|  | Before lyophilization | After lyophilization |  |  |  |  |  |  |
| Zavg (nm) | 196.368 ± 1.123 | 198.357 ± 1.004 |  |  |  |  |  |  |
| PDI | 0.185 ± 0.001 | 0.193 ± 0.002 |  |  |  |  |  |  |
| ζ (mV) | - 23.6 ± 1.355 | -23.14 ± 0.897 |  |  |  |  |  |  |
| Entrapment efficiency (EE) | 88.545 ± 2.134 | 86.359 ± 1.364 |  |  |  |  |  |  |
| Loading Capacity (LC) | 9.506 ± 0.223 | 9.266 ± 0.643 |  |  |  |  |  |  |

Results are presented as Mean ± SD

## Formulation of transgelosome (TFG), placebo TFG, and plain gel

The composition of transgelosomes (TFG F1-F3), placebo transgelosome (Placebo TFG F2), and plain gel is shown in Table S9.

Table S9 Composition of transgelosomes, placebo transgelosome, and plain gel

| Ingredients | Formulations |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | TFG F1 | TFG F2 | TFG F3 | Placebo TFG F2 | Plain Gel |
| PLFEE (mg) | -- | -- | -- | -- | 250 |
| Xanthan Gum (% w/v) | 1 | 3 | 5 | 3 | 3 |
| Methyl Paraben (% w/w) | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 |
| Propyl Paraben (% w/w) | 0.05 | 0.05 | 0.05 | 0.05 | 0.05 |
| Propylene glycol (% w/w) | 12.5 | 12.5 | 12.5 | 12.5 | 12.5 |
| 250 mg PLFEE loaded optimized transferosome (optimized TFs) (mL) | 10 | 10 | 10 | -- | -- |
| Placebo optimized TFs (mL) | -- | -- | -- | 10 | -- |
| Water (mL) | -- | -- | -- | -- | 10 |

TFG F1-F3 Transgelosomes formulations with different concentrations of Xanthan gum; Placebo TFG F2: placebo transgelosome

## Evaluation of gel formulations

Table S10 represents the characterization outcomes of the prepared gel formulations.

Table S10 Characterization of transgelosome, plain gel, and placebo transgelosome

| Formulations | TFG F1 | TFG F2 | TFG F3 | Placebo TFG F2 | Plain Gel | Omnigel |
| --- | --- | --- | --- | --- | --- | --- |
| Appearance | White color | White color | White color | White color | Pale yellow | White color |
| Consistency and homogeneity | Gel like consistency with smooth and homogeneous properties | Gel like consistency with smooth and homogeneous properties | Gel like consistency with smooth and homogeneous properties | Gel like consistency with smooth and homogeneous properties | Gel like consistency with smooth and homogeneous properties | Gel like consistency with smooth and homogeneous properties |
| Spreadability (cm) | 5.467 ± 0.047 | 5.034 ± 0.048 | 4.547 ± 0.031 | 5.103 ± 0.091 | 5.23 ± 0.089 | 4.941 ± 0.417 |
| Extrudability (g) | 141.217 ± 2.157 | 154.372 ± 1.428 | 164.739 ± 2.357 | 150.367 ± 1.445 | 146.125 ± 2.147 | 155.847 ± 1.665 |
| pH | 6.725 ± 0.051 | 6.736 ± 0.018 | 6.682 ± 0.023 | 6.279 ± 0.041 | 6.652 ± 0.035 | 6.67 ± 0.035 |
| Viscosity (mPa.s) at Shear rate of 25.1/sec | 101.203 ± 2.117 | 450.042 ± 3.464 | 847.16 ± 3.837 | 426.31 ± 2.643 | 407.73 ± 2.137 | 464.19 ± 2.432 |
| Drug content (%) | 98.356 ± 1.258 | 98.647 ± 1.124 | 97.899 ± 2.237 | 0 | 98.436 ± 1.159 | -- |
| Syneresis (%) | 1.834 ± 0.012 | 0.671 ± 0.001 | 0.554 ± 0.0.004 | 0.832 ± 0.002 | 0.941 ± 0.003 | 0.604 ± 0.001 |

Results were represented as mean ± standard deviation (n = 3)

TFG F1-F3 Transgelosomes formulations with different concentrations of Xanthan gum; Placebo TFG F2: placebo transgelosome

## Compatibility study of gel

The compatibility among extract and excipients in the gel formulation evaluated by ATR-FTIR spectroscopy was shown in Figure S9.

Figure S9    ATR-FTIR study of gel formulations, formulation components, and physical mixture for drug-excipient compatibility analysis

PLFEE: Piper longum fruits ethanolic extract; Phy Mix Plain Gel: physical mixture of plain gel; Plain Gel FD: Freeze-dried plain gel; Phy Mix of TFG: physical mixture of transgelosome; TFG F1-3 FD: freeze-dried Transgelosome formulations (F1-F3); Placebo TFG F2 FD: freeze-dried placebo transgelosome of F2

## Kinetics of drug release

The Kinetics of drug release from optimized TFs and TFG F2 were shown in Table S11.

Table S11 Kinetics of drug release from optimized TFs and TFG F2

|  |  | Zero-order |  | First-order |  | Higuchi Model |  | Korsmeyer-Peppas model |  | Hixson-Crowell model |  |  | Mechanism of drug release |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | K0 | R2 | K1 | R2 | KH | R2 | Kkp | R2 | KHC | R2 | n |  | R2 |
|  | optimized TFs | 1.420 | 0.726 | 0.015 | 0.878 | 11.115 | 0.901 | 0.408 | 0.898 | 0.038 | 0.558 | 0.541 |  | 0.913 |
|  | TFG F2 | 0.998 | 0.763 | 0.007 | 0.857 | 7.686 | 0.916 | 0.338 | 0.906 | 0.033 | 0.578 | 0.388 |  | 0.906 |
| Drug permeation across the skin |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | TFG F2 | 1.993 | 0.980 | 0.016 | 0.983 | 13.466 | 0.987 | 0.613 | 0.977 | 0.067 | 0.861 | 0.599 |  | 0.970 |

## Stability study of gel

The stability of TFG F2 and plain gel with respect to various physicochemical parameters evaluated under long-term stability conditions (5 ± 3°C) and accelerated conditions (25 ± 2°C/60 ± 5% RH) were shown in Table S12 and Table S13, respectively.

Table S12 Long-term stability study of prepared hydrogels under refrigerated conditions (5 ± 3°C)

| Formulations | TFG F2 |  |  |  | Plain Gel |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0 month | 6 months | 9 months | 12 months | 0 month | 3 months | 6 months | 12 months |
| Appearance | White color |  |  |  | Pale yellow |  |  |  |
| Consistency and homogeneity | Gel-like consistency with smooth and homogeneous properties |  |  |  | Gel-like consistency with smooth and homogeneous properties |  |  |  |
| Spreadability (cm) | 5.034 ± 0.048 | 5.012 ± 0.014 | 4.998 ± 0.079 | 4.986 ± 0.035 | 5.23 ± 0.089 | 5.211 ± 0.057 | 5.167 ± 0.037 | 5.087 ± 0.033 |
| Extrudability (g) | 154.372 ± 1.428 | 153.751 ± 1.547 | 155.368 ± 1.764 | 157.2 ± 1.258 | 146.125 ± 2.147 | 147.284 ± 1.234 | 147.873 ± 1.354 | 148.325 ± 1.359 |
| pH | 6.736 ± 0.018 | 6.657 ± 0.038 | 6.773 ± 0.024 | 6.623 ± 0.014 | 6.652 ± 0.035 | 6.643 ± 0.134 | 6.653 ± 0.032 | 6.623 ± 0.072 |
| Viscosity (mPa.s) at a Shear rate of 25.1/sec | 450.042 ± 3.464 | 452.034 ± 2.346 | 452.132 ± 2.657 | 450.3344 ± 3.214 | 407.73 ± 2.137 | 407.123 ± 3.211 | 406.357 ± 2.244 | 407.133 ± 3.338 |
| Drug content (%) | 98.647 ± 1.124 | 98.253 ± 1.233 | 98.147 ± 1.243 | 97.221 ± 1.225 | 98.436 ± 1.159 | 98.124 ± 1.287 | 97.369 ± 1.118 | 97.123 ± 2.134 |
| Syneresis (%) | 0.671 ± 0.001 | 0.682 ± 0.002 | 0.686 ± 0.001 | 0.693 ± 0.003 | 0.941 ± 0.003 | 0.944 ± 0.002 | 0.953 ± 0.001 | 0.986 ± 0.002 |
| Drug-excipient compatibility | Compatible |  |  |  | Compatible |  |  |  |

Results are presented as Mean ± SD

Table S13 Accelerated stability study of prepared hydrogels at 25 ± 2°C/60 ± 5% RH

| Formulations | TFG F2 |  |  | Plain Gel |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0 month | 3 months | 6 months | 0 month | 3 months | 6 months |
| Appearance | White color |  |  | Pale yellow |  |  |
| Consistency and homogeneity | Gel-like consistency with smooth and homogeneous properties |  |  | Gel-like consistency with smooth and homogeneous properties |  |  |
| Spreadability (cm) | 5.034 ± 0.048 | 4.987 ± 0.035 | 4.873 ± 0.037 | 5.23 ± 0.089 | 5.156 ± 0.027 | 5.024 ± 0.044 |
| Extrudability (g) | 154.372 ± 1.428 | 156.545 ± 2.334 | 158.357 ± 1.887 | 146.125 ± 2.147 | 147.317 ± 2.753 | 149.354 ± 1.738 |
| pH | 6.736 ± 0.018 | 6.735 ± 0.075 | 6.686 ± 0.055 | 6.652 ± 0.035 | 6.655 ± 0.103 | 6.631 ± 0.047 |
| Viscosity (mPa.s) at a Shear rate of 25.1/sec | 450.042 ± 3.464 | 455.754 ± 2.117 | 457.454 ± 2.786 | 407.73 ± 2.137 | 410.557 ± 3.154 | 412.857 ± 2.244 |
| Drug content (%) | 98.647 ± 1.124 | 97.754 ± 2.225 | 97.346 ± 1.633 | 98.436 ± 1.159 | 97.368 ± 1.354 | 96.843 ± 2.433 |
| Syneresis (%) | 0.671 ± 0.001 | 0.697 ± 0.003 | 0.712 ±0.002 | 0.941 ± 0.003 | 0.988 ± 0.001 | 0.997 ± 0.003 |
| Drug-excipient compatibility | Compatible |  |  | Compatible |  |  |

Results are presented as Mean ± SD

## Ex-vivo skin permeation study

The results of the permeability coefficient (Kp), steady state flux (Jss), enhancement ratio (Er), and maximum flux (Jmax) were shown in Table S14.

Table S14 Ex-vivo skin permeability of plain gel and transgelosome (TFG F2)

| Gel | Permeability coefficient (Kp) | Steady-state Flux (Jss) | Enhancement Ratio (ER) | Maximum Flux (Jmax) |
| --- | --- | --- | --- | --- |
|  | (h-1.cm-2) | (µg. h-1.cm-2) |  | (µg. h-1.cm-2) |
| Plain gel | 0.0012 | 1.935 ± 0.057 | -- | 6.791 ± 0. 645 |
| TFG F2 | 0.0026 | 4.332 ± 0.243 | 2.238 | 13.489 ± 0. 753 |

Results were represented as mean ± standard deviation (n = 3)

Figure S10 Structure of skin and the penetration mechanism of transferosome across the skin (A) anatomy of the skin, and (B) mechanism of skin penetration of ultradeformable transferosome

## Acute dermal toxicity and skin irritation study

The outcomes of the dermal toxicity study of standardized PLFEE were reported based on survival or death, skin color (Draize criteria), change in body weight, behavioral alterations, hematological parameters, biochemical parameters, and histopathology. The skin irritation potential of prepared hydrogels was reported based on the Draize criteria. No death of animals was noticed at any topical dose (200, 1000, and 2000 mg/kg) of standardized PLFEE after 14 days. The photographs of vehicle-applied control C57BL/6 female mouse and standardized PLFEE (2000 mg/kg) applied C57BL/6 mouse was shown in Figure S11A and Figure S11B, respectively. After topical application (after 30 min) of standardized PLFEE, a disagreeable rapid movement of animals was observed without any visual sign of skin irritation (erythema or edema). The disagreeable behavior was ascribed to the pungent principle of standardized PLFEE. Table S15 represents the grading values for the primary skin irritation test and the corresponding response categories as per Draize criteria. The values (zero) of the average primary irritation index (PII) by the standardized PLFEE (2000 mg/kg) are the same as that of the vehicle-treated C57BL/6 group (Table S16), representing its non-irritancy nature. The skin histopathological observations of vehicle-applied control C57BL/6 female mouse (Figure S11C), and standardized PLFEE (2000 mg/kg) applied C57BL/6 mouse (Figure S11D) showed no alterations of the skin anatomy. The changes in the body weight between the vehicle (water) control group (21.843 ± 2.658 g) and standardized PLFEE (2000 mg/kg) treated animals (22.138 ± 1.157 g) were found to be statistically insignificant (p<0.05) on 14th day. The biochemical parameters (Table S17) and hematological parameters (Table S18) of the aforementioned groups, studied after 14 days, reflected a non-significant difference (p<0.05).

The vital organs’ histology of the vehicle-treated group (Figure S12A) and standardized PLFEE (2000 mg/kg) applied C57BL/6 group (Figure S12B) displayed branching myocytes (BM) of the heart, glomerulus (G) of the kidney, central vein (CV), and hepatic portal vein (HPV) of the liver; bronchioles (B) of the lungs, red pulp (RP) and white pulp (WP) of the spleen. No histological changes of the vital organs were observed from the histological photomicrographs of the vehicle-applied control C57BL/6 mice group (Figure S12A) and standardized PLFEE (2000 mg/kg) applied C57BL/6 mice group (Figure S12B). The overall outcomes of the acute dermal toxicity study revealed no sign of dermal toxicity in the C57BL/6 animals after topical application of standardized PLFEE even at a higher dose (2000 mg/kg) and signifying its possible pre-clinical applicability.

Figure S11 Acute dermal toxicity study for estimation of skin irritancy (A) photograph of vehicle applied control C57BL/6 female mouse, (B) photograph of standardized PLFEE (2000 mg/kg) applied C57BL/6 mouse, (C) histopathology of vehicle applied control C57BL/6 female mouse, and (D) histopathology of standardized PLFEE (2000 mg/kg) applied C57BL/6 mouse observed at 10X magnification

Table S15 Grading values for the primary skin irritation test and response categories

| Skin responses | Score of primary irritation index (PII) |
| --- | --- |
| Erythema and Eschar Formation |  |
| - No Erythema | 0 |
| - Very slight erythema (barely perceptible) | 1 |
| - Well-defined erythema | 2 |
| - Moderate to severe erythema | 3 |
| - Severe erythema (beet-redness) to slight eschar formation (injuries in depth) | 4 |
| Edema formation |  |
| - No edema | 0 |
| - Very slight edema (barely perceptible) | 1 |
| - Slight edema (edges of area well-defined by definite raising) | 2 |
| - Moderate edema (raised approximately 1.0 mm) | 3 |
| - Severe edema (raised more than 1.0 mm and extending beyond the area of exposure) | 4 |
| Total possible score for irritation | 8 |
| Primary irritation index (PII) | Category |
| - 0 - 0.4 | Negligible |
| - 0.5 - 1.9 | Slight irritation |
| - 2.0 - 4.9 | Moderate irritation |
| - 5.0 - 8.0 | Severe irritation |

Table S16 Reaction on skin and score of vehicle-applied control C57BL/6 female mice, and standardized PLFEE (2000 mg/kg) applied C57BL/6 mice

| Formulation | Response | After time interval (h) | C57BL/6 mice |  |  |  | PII Score | Category |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | i | ii | iii | iv |  |  |
| Vehicle applied | Erythema | 24 | 0 | 0 | 0 | 0 | 0 |  |
|  |  | 48 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  |  | 72 | 0 | 0 | 0 | 0 | 0 |  |
|  | Edema | 24 | 0 | 0 | 0 | 0 | 0 |  |
|  |  | 48 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  |  | 72 | 0 | 0 | 0 | 0 | 0 |  |
| Standardized PLFEE (2000 mg/kg) applied | Erythema | 24 | 0 | 0 | 0 | 0 | 0 |  |
|  |  | 48 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  |  | 72 | 0 | 0 | 0 | 0 | 0 |  |
|  | Edema | 24 | 0 | 0 | 0 | 0 | 0 |  |
|  |  | 48 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  |  | 72 | 0 | 0 | 0 | 0 | 0 |  |

PII: Primary irritation index

Table S17 Biochemical parameters of topically applied vehicle control C57BL/6 group and standardized PLFEE (2000 mg/kg) treated C57BL/6 group

| Serum biochemical parameters | Vehicle control C57BL/6 group | PLFEE (2000 mg/kg) treated C57BL/6 group |
| --- | --- | --- |
| Creatinine (mg/dL) | 0.31 ± 0.031 | 0.34 ± 0.018 |
| Urea (mg/mL) | 40.37 ± 3.158 | 41.48 ± 3.163 |
| ALP (U/L) | 46.23 ± 3.784 | 44.55 ± 2.436 |
| SGPT (U/L) | 35.85 ± 3.565 | 36.132 ± 2.463 |
| SGOT (U/L) | 138.7 ± 0.312 | 136.2 ± 0.372 |
| Total Cholesterol (mg/dL) | 90.46 ± 3.466 | 92.513 ± 2.371 |
| Triglyceride(mg/dL) | 105.2 ± 2.498 | 103.72 ± 3.617 |
| Glucose (mg/dL) | 220 ± 9.748 | 222 ± 6.751 |
| Total protein (g/dL) | 6.892 ± 0.131 | 7.134 ± 0.533 |

ALP: alkaline phosphatase, SGPT: serum glutamic pyruvic transaminase, SGOT: serum glutamic-oxaloacetic transaminase

Students t-test was performed at p<0.05 using GraphPad Prism 5 (GraphPad Software, Inc., San Diego, California).

Table S18 Hematological parameters of topically applied vehicle control C57BL/6 group and standardized PLFEE (2000 mg/kg) treated C57BL/6 group

| Hematological parameters | Vehicle control C57BL/6 group | PLFEE (2000 mg/kg) treated C57BL/6 group |
| --- | --- | --- |
| TLC/ WBC (*103/µL) | 4.2 ± 0.732 | 3.9 ± 0.563 |
| Hemoglobin (gm/dL) | 13.1 ± 2.435 | 12.3 ± 2.498 |
| Monocytes (%) | 6 ± 1.247 | 7 ± 1.023 |
| Lymphocytes (%) | 57 ± 8.123 | 57 ± 7.423 |
| Neutrophils (%) | 35 ± 2.336 | 34 ± 3.643 |
| Eosinophils (%) | 2 ± 0.435 | 2 ± 0.543 |
| Basophils (%) | 0 | 0 |
| TRBCs (×106/ µL) | 9.27 ± 0.425 | 9.17 ± 0.373 |
| PCV (%) or HCT (%) | 40.3 ± 4.753 | 41.369 ± 5.356 |
| RDW (%) | 15.7 ± 3.243 | 15.643 ± 2.46 |
| MCV (fL) | 44.0 ± 5.776 | 43.5 ± 4.147 |
| MCH (pg) | 13.5 ± 3.436 | 14.3 ± 2.435 |
| MCHC (g/dL) | 32.6 ± 4.573 | 31.5 ± 3.363 |
| Platelet (×105/ µL) | 5.34 ± 0.382 | 4.956 ± 0.283 |

TLC: total leucocyte count, WBC: white blood cells, TRBCs: total red blood cell counts, PCV: packed cell volume or HCT: hematocrit test, RDW: red cell distribution width, MCV: mean corpuscular volume, MCH: mean corpuscular haemoglobin, MCHC: mean corpuscular haemoglobin concentration

Students t-test was performed at p<0.05 using GraphPad Prism 5 (GraphPad Software, Inc., San Diego, California).

Figure S12 Histopathology of heart, kidney, liver, lungs, and spleen of (A) vehicle control C57BL/6 group and (B) PLFEE (2000 mg/kg) topically treated C57BL/6 group at 10X magnification for acute dermal toxicity assessment.

PLFEE: Piper longum fruits ethanolic extract; BM: branching myocytes; G: glomerulus; CV: central vein; HPV: hepatic portal vein; B: bronchioles: RP: and red pulp; and WP: white pulp

The visual outcomes of the skin irritation study were represented in Figure S13, and the corresponding erythema and edema scores of the study observed at 24, 48, and 72 h were shown in Table S19. The standard irritant (0.8% w/v aqueous formalin solution) showed a noticeable sign of skin irritation (Figure S13A) in C57BL/6 mice. The total PII scores (erythema + edema) indicate moderate to severe irritation by the standard irritant (Table S19). In contrast, the placebo gel (TFG F2) and all other gel formulations did not show any sign of skin irritation (Figure S13B-D). In the case of standardized PLFEE-loaded plain gel, a rapid moment of animals was observed after 30 minutes of topical application without any visual sign of skin irritation. Such behavior of the animals is ascribed to the pungency principle of PLFEE owing to the direct contact with the skin. However, in the case of vesicular gel (TFG F2), such behavior was not noticed, which is due entrapment of PLFEE inside the transferosomal vesicle. The histopathological photomicrograph of skin treated with standard irritant showed ruptured anatomy (Figure S14A). In contrast, the photomicrographs of skin topically applied with placebo TFG F2, TFG F2, and plain gel showed intact skin architecture of distinct layers of skin (epidermis, dermis, and hypodermis) with no deterioration or anatomical alterations (Figure S14B-D).  A topical product with higher acidity or alkalinity affects the natural environment of the skin [5-7]. All the formulated gels possess a pH towards neutrality, hence having very less chance of skin irritation due to acidity and alkalinity. The overall results indicated the acceptable skin tolerability of the prepared gels.

Figure S13 Skin irritation study of (A) standard irritant (0.8% w/v aqueous formalin solution), (B) placebo TFG F2, (C) TFG F2, and (D) plain gel

Placebo TFG F2: Placebo transgelosome formulation TFG F2; TFG F2: Transgelosome containing optimized transferosome

Table S19 Reaction on skin and score of standard irritant (0.8% v/v aqueous formalin solutions),

placebo TFG-F2 (vehicle control), TFG-F2, and plain gel on femaleC57BL/6 mice

| Formulation | Time (h) | PII of Erythema |  |  |  | Average PII score of Erythema (a) | PII of Edema |  |  |  | Average PII score of Edema (b) | Total irritation score (a + b) | Category |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | i | ii | iii | iv |  | i | ii | iii | iv |  |  |  |
|  | 24 | 3 | 3 | 4 | 3 | 3.250 | 2 | 2 | 1 | 2 | 1.750 | 5 | Severe irritation |
| Standard irritant | 48 | 2 | 2 | 3 | 2 | 2.250 | 1 | 1 | 1 | 0 | 0.750 | 3 | Moderate irritation |
|  | 72 | 2 | 2 | 2 | 1 | 1.75 | 1 | 1 | 0 | 0 | 0.500 | 2.250 | Moderate irritation |
|  | 24 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
| Placebo TFG F2 | 48 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  | 72 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | 24 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
| TFG F2 | 48 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  | 72 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | 24 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
| Plain Gel | 48 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | Negligible |
|  | 72 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |

PII: Primary irritation index

Figure S14 Histopathological photomicrographs of C57BL/6 mice skin after skin irritation studies of (a) standard irritant (0.8% w/v aqueous formalin solution), (b) placebo TFG F2, (c) TFG F2, and (d) plain gel

## Histopathology of tumors

The histopathological photomicrographs of healthy skin, skin over melanoma tumor, and tumor tissues from female C57BL/6 mice of tumor control and various treatment groups were shown in Figure S15. The histology of healthy skin (Figure S15A) represented distinct layers of epidermis, dermis, and hypodermis, representing the normal anatomy of the skin. However, the photomicrograph of skin over melanoma (Figure S15B) displayed destroyed anatomy and the presence of live tumor cells (LTC). The “Tumor control” group presented a larger population of LTC (Figure S15C). In contrast, all the treatment groups displayed a reduced population of the LTC (Figure S15D-S15H).  The “Plain gel” group displayed few necrotic regions (NR) with a reduction of LTC. The TFG F2 applied group- showed a marked reduction of LTC with a relatively higher population of NR. The DTIC alone caused a noticeable decrease in the LTC population as an antineoplastic drug. Further, a marked reduction of the LTC was observed in the case of the “DTIC + Plain gel” group with a relatively larger necrotic area. The “DTIC + TFG F2” group demonstrated a very low population of LTC and larger NR compared to the “DTIC + Plain gel” group. The overall outcomes presented the higher anticancer activity of standardized PLFEE-loaded TFG F2 compared to the plain gel. Further, TFG F2 as an adjuvant treatment will improve the activity of DTIC for melanoma therapy.

Figure S15 Histopathology study of skin and melanoma tumor: histology of (A) normal skin, (B) skin over melanoma tumor, (C) tumor of tumor control, (D) tumor of DTIC treated, (E) tumor ofplain gel, (F) tumor of TFG F2treated, (G) tumor of DTIC + Plain geltreated, and (H) tumor of DTIC + TFG F2treated group. NR: necrotic region; LTC: live tumor cell

References

1.	Guideline IHT. Validation of analytical procedures: text and methodology Q2 (R1). Presented at: International conference on harmonization of technical requirements for registration of pharmaceuticals for human use. 2005.

2.	Pitta SK, Dudhipala N, Narala A, Veerabrahma K. Development of zolmitriptan transfersomes by Box–Behnken design for nasal delivery: in vitro and in vivo evaluation. Drug Dev Ind Pharm 44(3), 484-492 (2018).

3.	Pramod K, Suneesh CV, Shanavas S, Ansari SH, Ali J. Unveiling the compatibility of eugenol with formulation excipients by systematic drug-excipient compatibility studies. J Anal Sci Technol 6(1), 1-14 (2015).

4.	Mohapatra D, Alam MB, Pandey V et al. Carbon dots from an immunomodulatory plant for cancer cell imaging, free radical scavenging and metal sensing applications. Nanomedicine 16(23), 2039-2059 (2021).

5.	Ahad A, Al-Saleh AA, Al-Mohizea AM et al. Pharmacodynamic study of eprosartan mesylate-loaded transfersomes Carbopol® gel under Dermaroller® on rats with methyl prednisolone acetate-induced hypertension. Biomed Pharmacother 89 177-184 (2017).

6.	El-Gizawy SA, Nouh A, Saber S, Kira AY. Deferoxamine-loaded transfersomes accelerates healing of pressure ulcers in streptozotocin-induced diabetic rats. J Drug Deliv Sci Technol 58 101732 (2020).

7.	Dixit K, Mohapatra D, Senapati P, Sahu A. Formulation Development and Evaluation of Lawsonia inermis Extract Loaded Hydrogel for Wound Dressing Application. Indian J Pharm Sci 84(4), 848-862 (2022).

8.	Khatoon K, Rizwanullah M, Amin S, Mir SR, Akhter S. Cilnidipine loaded transfersomes for transdermal application: formulation optimization, in-vitro and in-vivo study. J Drug Deliv Sci Technol 54 101303 (2019).

9.	Dudhipala N, Phasha Mohammed R, Adel Ali Youssef A, Banala N. Effect of lipid and edge activator concentration on development of aceclofenac-loaded transfersomes gel for transdermal application: In vitro and ex vivo skin permeation. Drug Dev Ind Pharm 46(8), 1334-1344 (2020).

10.	Ding Y, Wang C, Wang Y et al. Development and evaluation of a novel drug delivery: Soluplus®/TPGS mixed micelles loaded with piperine in vitro and in vivo. Drug Dev Ind Pharm 44(9), 1409-1416 (2018).

11.	Shuwaili AHA, Rasool BKA, Abdulrasool AA. Optimization of elastic transfersomes formulations for transdermal delivery of pentoxifylline. Eur J Pharm Biopharm 102 101-114 (2016).

12.	Das B, Sen SO, Maji R, Nayak AK, Sen KK. Transferosomal gel for transdermal delivery of risperidone: Formulation optimization and ex vivo permeation. J Drug Deliv Sci Technol 38 59-71 (2017).

13.	Allaw M, Pleguezuelos-Villa M, Manca ML et al. Innovative strategies to treat skin wounds with mangiferin: Fabrication of transfersomes modified with glycols and mucin. Nanomedicine 15(17), 1671-1685 (2020).

14.	Habib BA, Sayed S, Elsayed GM. Enhanced transdermal delivery of ondansetron using nanovesicular systems: fabrication, characterization, optimization and ex-vivo permeation study-Box-Cox transformation practical example. Eur J Pharm Sci 115 352-361 (2018).

15.	González-Rodríguez M, Arroyo C, Cózar-Bernal M et al. Deformability properties of timolol-loaded transfersomes based on the extrusion mechanism. Statistical optimization of the process. Drug Dev Ind Pharm 42(10), 1683-1694 (2016).

16.	Elkomy MH, El Menshawe SF, Abou-Taleb HA, Elkarmalawy MH. Loratadine bioavailability via buccal transferosomal gel: formulation, statistical optimization, in vitro/in vivo characterization, and pharmacokinetics in human volunteers. Drug Deliv 24(1), 781-791 (2017).

17.	Tsubaki M, Takeda T, Obata N et al. Combination therapy with dacarbazine and statins improved the survival rate in mice with metastatic melanoma. J. Cell. Physiol. 234(10), 17975-17989 (2019).

18.	Pandey S. In vivo antitumor potential of extracts from different parts of Bauhinia variegata linn. Against b16f10 melanoma tumour model in c57bl/6 mice. Applied Cancer Research 37(1), 1-14 (2017).