**Table S14** *Ex-vivo* skin permeability of plain gel and transgelosome (TFG F2)

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Gel | Permeability coefficient (Kp) | Steady-state Flux (Jss) | Enhancement Ratio (ER) | Maximum Flux (Jmax) |
|  | (h-1.cm-2) | (µg. h-1.cm-2) |  | (µg. h-1.cm-2) |
| Plain gel | 0.0012 | 1.935 ± 0.057 | -- | 6.791 ± 0. 645 |
| TFG F2 | 0.0026 | 4.332 ± 0.243 | 2.238 | 13.489 ± 0. 753 |

Results were represented as mean ± standard deviation (n = 3)