Supplementary Documents

Efficient Synthesis of Glyco Disulphide Capped Gold Nanoparticles: Cytotoxicity Studies, and Effects on Lung Cancer A549 Cells

Christian K. Adokoh‡, Franklin K. Keter†#, Collins Obuah§, Henok H. Kinfe‡, Robert Tshikhudo† and James Darkwa‡

‡Department of Chemical Sciences, University of Johannesburg, P. O. Box 524, Auckland Park, 2006, South Africa

†Nanotechnology Innovation Center, Advanced Materials Division, Mintek, 200 Malibongwe Drive, Randburg, 2125, South Africa

§Department of Chemistry, University of Ghana, Legon, Ghana.

ΨCurrent Address: Department of Forensic Sciences, University of Cape Coast, College of Agriculture and Natural Sciences, School of Biological Sciences.

#Current Address: Clinton Health Access Initiative, P. O. Box 2011-00100, Nairobi, Kenya

Direct Method of Synthesis of Glyco Disulfide AuNPs

The UV-vis data of AuNPs GD2 showed sharp intense peaks between 529-538 nm at high pH and broad peaks 536-554 nm at low pH (Figure S1a-b) indicating aggregation of particles.

b.

a.

Figure S1: UV-vis spectrometer of GD2 AuNP (a) Low pH 8.9-9.2 (b) High pH (12.4-12.5)

d

e

f

e

f

d

Figure S2: (d-f) TEM micrograph of AuNP GD2 with Au:L2 ratio of 1: 0.5, 1:1 and 1: 1.5 respectively at various ligand pHs. Note: d´-f´ are TEM micrograph of a-c at pH ~12 respectively

S-S

Figure S3a: Raman spectrum of gluconamidoethyl disulfide (L1)

Au-S bond

Up field shift of S-S bond

Figure S3b: Raman spectrum of gluconamidoethyl disulfide AuNP via direct method

Au-S bond

Up field shift of S-S bond

Figure S3c: Raman spectrum of gluconamidoethyl disulfide AuNP via ligand exchange

Figure S4: UV-vis spectrum of GD1 AuNP at different pHs.

Synthesis of Non-acetylated and Acetylated Disulfide Gluconamidoalkyl AuNPs (GD4-9) via Substitution Method

Figure S5: General representation of substitution gold nanoparticles synthesis.

Photochemical Irradiation Synthesis of Gluconamidoalkyl Disulfide Gold Nanoparticles (GD10-16)

The monodispersed cationic glyconanoparticle was synthesized in situ via photochemical irradiation method using photoinitiator Irgacure 2959 (Figure S6).  The gold nanoparticles were prepared in double distilled water with ratios of HAuCl4: IRGC: gluconamidoalkyl disulfides (L1-L3) (1:3:1 and 1:3:1.5).

.

Figure S6: Preparation of glyco disulfide gold nanoparticles via photochemical irradiation method.

TEM image of the following photoirradiation of various ratios of ligands to gold are presented in the figure S7 below.

d

c

a

b

e

f

Figure S7: TEM image of GNP of (a) aggregated GD14   (b) aggregated GD15 (c) GD11 (d) GD12 (e, f) GD13.

In vitro anticancer screening of gold disulfide glyconanoparticles

Two cell lines: Human normal peripheral blood mononuclear cells (PBMCs) and Human lung adenocarcinoma epithelial cell line (A549) were used to study the cytotoxicity activities of selected disulfide gold glyconanoparticles (GD1- GD3, GD4, GD6 and GD7). The figure below demonstrates growth inhibition profile of A549 cancer cells of the AuNPs GD1.

0.0

0.8

1.6

0.5

1.0

1.5

2.0

Abs (450/800 nm)

Log(Compound conc.) (µg/mL)

Figure S8. Growth inhibition profile of A549 cancer cells by AuNPs GD1

corresponding author’s address: Current Address: Department of Forensic Sciences, University of Cape Coast, College of Agriculture and Natural Sciences, School of Biological Sciences (Email: cadokoh@ucc.edu.gh) Tel. +233264769777

‡Department of Chemistry, University of Johannesburg, P. O. Box 524, Auckland Park, 2006, South Africa. (Email: jdarkwa@gmail.com) Tel. +27728524639, +23326772816153